Directed Energy Deposition of Metals: Processing, Microstructures and Mechanical Properties

Shihao Li a, Punit Kumar a, Shubham Chandra a, Upadrasta Ramamurty a, b,*

a School of Mechanical and Aerospace Engineering, Nanyang Technological University, Singapore 639798, Republic of Singapore

b Institute of Materials Research and Engineering, Agency for Science, Technology and Research, 2 Fusionopolis Way, Singapore 138634, Republic of Singapore

Corresponding author’s address: uram@ntu.edu.sg (U. Ramamurty)

Abstract: Directed energy deposition (DED), as integral component of additive manufacturing (AM), has achieved continuous progress in past decades and is now performing as promising alternative manufacturing technology for components employed in various industrial applications. This review paper describes DED technique, presents typical microstructure evolution and discusses mechanical responses of DED components upon different loadings. Microstructures and mechanical properties of commercially available materials, including steels, Ti alloys and Ni-based superalloys, are presented in detail and compared to their conventionally manufactured (CM) and laser beam powder bed fusion (LB-PBF) counterparts. In addition, the relationship among processing, microstructures and properties is explored based on available DED studies to gain in-depth understanding of DED technique. The application of DED on manufacturing of functionally graded materials (FGM) and component repair is elaborated with special concentration on issues encountered and possible solutions. Finally, some critical issues and research needs to help develop DED and extend its applications are discussed.

Keywords: Directed energy deposition, processing, microstructures, mechanical properties

Nomenclature

AM       			additive manufacturing

AT                 		aging treatment

BCC      			body-centered cubic

CAD      			computer aid design

CET      		columnar to equiaxed transition

CM                		conventionally manufactured

DED   			directed energy deposition

EBSD     			electron backscatter diffraction

EDS      			energy dispersive X-ray spectroscopy

FCC       			face-centered cubic

FGM      			functionally graded materials

GND      			geometrically necessary dislocation

GB      			grain boundary

HAGB    			high angle grain boundary

HCF      			high cyclic fatigue

HIP       			hot isostatic pressing

HSAT              		homogenization, solution, and aging treatment

LAGB     			low angle grain boundary

LB-PBF          			laser beam powder bed fusion

LCF      			low cyclic fatigue

LoF      			lack-of-fusion

M                                     	martensite

PCAS     			primary cellular arm spacing

PFS       			powder-feeding system

PH       			precipitation hardening

SAT               			solution and aging treatment

SEM      			scanning electron microscopy

SS        			stainless steel

ST                 		solution treatment

STEM     			scanning transmission electron microscopy

TEM      			transmission electron microscopy

UTS      			ultimate tensile strength

WFS      			wire-feeding system

XRD      			X-ray diffraction

A                                       	anisotropy index

AY                                     	anisotropy in yield strength

Aε                                     	anisotropy in elongation

DL        			diffusion coefficient of solute in liquid

Eg                 		global energy density

El        			linear heat input

En                                     	normalized energy density

Ev        			volumetric energy density

G         			temperature gradient

N0        			number of nucleation sites

P         			heat source energy

R         			solidification rate

Ra                 		surface roughness

T         			cooling rate

d                  		laser spot size

h         			layer thickness

λ         			primary cellular arm spacing

γ                                        	austenite

δ                                        	ferrite

w                 			width of single track

εf                                      	elongation at failure

φ         			volume fraction of equiaxed grains

v         			scanning speed

σh        			tensile properties along horizontal direction

σv        			tensile properties along vertical direction

σY        			yield strength

σUTS                                  	ultimate tensile strength

- Introduction

Additive manufacturing (AM), widely known as three dimensional (3D) printing, produces near-net-shape components of the desired geometry in a layer-wise fashion using the computer aided design (CAD) models [1][2-4]. Amongst the several advantages AM offers, the ability to manufacture parts with complex designs, often using only one processing step combined with the minimum wastage of the raw material, is perhaps the most attractive feature [1-3]. As a result, considerable current interest on it—both from research and technological perspectives—for wide ranging applications in automotive, marine, aerospace, and biomedical fields exists [1-4].

This review’s focus is on AM of metallic components, and, in particular, using the directed energy deposition (DED) technique. A variety of methodologies for metal AM are being pursued over the past few years. Amongst them, those which use powders as the raw materials are the most popular. These can be categorised into three distinct groups. In the powder bed fusion (PBF)-based techniques, either a laser (LPBF) or an electron beam (EPBF) is used to fuse, line-by-line and then layer-by-layer, selected areas of the powder beds to fabricate the desired part [6, 7]. By far, these are the most widely explored metal AM techniques. While the binder jet printing (BJP) also uses a powder bed, it differs in the working principle (and hence is considered as an indirect method). In it, a polymer-based binder is used to bond the powder particle in the desired areas of the powder beds; the ‘green’ preform is then sintered to remove the binder and fuse the metal particles. On the other hand, DED does not involve powder beds; rather the feedstock material (in most cases, powder), which is injected through the energy beam’s focal point, melts during the flight before being deposited on the substrate. More details and the relative advantages/drawbacks of it over the other AM techniques are provided in the next section. Due to certain unique advantages it offers, AM using DED is drawing increasing interest—both from scientific and technological perspectives—and DED of a variety of metallic materials such as steels, Ti-based lightweight alloys, and Ni-based superalloys [15-17] are being studied with focus on the thermal history, microstructure, and mechanical property relations [19-22]. They reveal heterogeneous, hierarchical, and anisotropic solidification structures, which differ from that of conventionally manufactured (CM) counterparts (and are also distinct from the other metal AM technique), in the DED components [17, 23]. The complex thermal history inherent to DED process, that varies significantly with materials, processing parameters and scanning strategies, is a key factor that determines the observed disparate microstructural characteristics [1, 23]. In the DED techinqie, the feedstock delivered to the molten pool is subjected to rapid melting and solidification followed by cyclic reheating. Due to the intrinsic rapid cooling rates, the solidification process is typically far from equilibrium, resulting in metastable microstructures (whose composition is non-equilibrium in nature) that are not feasible within CM counterparts [1-3, 23]. The disparate microstructures (such as columnar grains, cellular structures, dispersed defects, etc.) impart unique mechanical behavior to the DED alloys [23-28].

A comprehensive understanding of relations among the process parameters, resulting microstructural characteristics, and the influence they exert on the mechanical performance of the DED alloys is yet to be developed. Keeping this in view, the available literature on DED alloys, with specific attention on the processing parameter optimization, microstructural characterization, and mechanical performance evaluation in DED alloys is reviewed in this paper.

This paper is organized in the following manner. A detailed description of the DED process and its relative merits (over LPBF, which is the most widely studied AM technique for metals) are provided in Section 2. Typical microstructural features in the DED alloy components are discussed in Section 3 and a summary of their mechanical properties is presented in Section 4. Some unique applications of DED techniques, including fabrication of FGMs and component repair, are discussed in Section 5. This review closes with the identification of future directions for research on this exciting AM technology (Section 6).

Compared to PBF [6, 7], DED is characterized by some advantages that make it more competitive for industrial applications [2, 8]. First, DED process is typically conducted with higher feedstock feeding rate and therefore lower lead time relative to other AM processes, exhibiting superior manufacturing efficiency [9]. Second, DED process enables production of large parts with dimensions at the level of several meters and weight of hundreds of kilograms [10, 11]. As for PBF, however, it is reported that volumes of deposited parts are typically less than 0.03 m3 due to limitation of a few factors, such as enclosed working envelope [2]. Third, DED process is compatible with various raw materials in terms of both powders and wires, while the feedstock for PBF is strictly constrained to powders. Fourth, functionally graded materials (FGMs), which are highly favorable in situations where part property variations with location are required, can be produced by DED process by adjusting the volume (or weight) fraction of constituent feedstock [12]. The high design freedom and flexibility in DED makes it possible to fabricate components with desired gradient in composition, microstructure and therefore properties. Finally, DED process is also suitable to be performed on selected substrate for the purpose of surface cladding and repair of damaged parts [13, 14].

- Working principle of DED and its advantages

2.1 DED process

A schematic of the working principle that is utilized in the DED techniques is illustrated in Fig. 1 [29]. The core idea in this process involves directing the feedstock material into a localized melt pool, which is created either on the surface of the substrate or the deposited layers by a heat source [30-37]. The heat source comprises primarily of laser [35, 38, 39], electron beam [40] and arc [31, 41, 42]. While both metallic wire and powder feedstock can be utilized for laser-based DED systems, electron beam and electric arc DED systems are strictly wire-based (Table 1 [21, 38-59]. Powder and wire-based DED process will be referred as powder-feed system (PFS) and wire-feed system (WFS), hereafter. Irrespective of the heating source, WFS is collectively termed as shaped metal deposition (SMD) [60] in which the feeding of the wire is done primarily via mechanical roller systems. In PFS, the feedstock is mixed with a carrier gas and delivered to the focal point of the laser on the part surface. An inert shielding gas is also utilized to generate a protective shroud around the melt pool [61]. The melting/solidification within the shielded envelope gives the powder based DED an edge over other metal AM techniques as it eliminates the need to use a completely inert environment – even enabling the capability to print underwater [62].

WFS, which can be regarded as the extension of the welding technology [63], has certain unique advantages over PFS, such as higher feed rate, shorter lead time, lower contamination, and capability to manufacture larger components [9-11, 51]. Martina and co-workers [9] proposed that the deposition rate of steels fabricated using WFS can be as high as 9.5 kg/h with a wire feeding rate of 9 m/min. In addition, successful fabrication of meter-scale Ti-based and Al-based components using WFS was demonstrated [10]. These sizes have been extended to 10 meters currently [11]. Moreover, WFS is highly cost effective (in comparison to PFS [18]) not only in terms of equipment and feedstock material cost, but also due to the usage of a mechanical roller in it (in comparison to an inert carrier gas – a consumable, in PFS). However, components manufactured using WFS suffer from high surface roughness, which mandates the post-process surface finishing through machining. Additionally, PFS has a major advantage over WFS for printing complex geometries and functionally graded parts [64, 65]. The microstructural evolution during the melt pool solidification in PFS is nearly independent of the feedstock microstructure – contrary to that in WFS. Therefore, significant alterations can be accomplished to achieve a desired microstructure in the 3D printed parts. Generally, PFS is the first choice for manufacturing near net shaped and intricate components with small to medium size, while WFS is a preferred for making components with low to medium complexity and medium to large dimensions.

2.2 Comparison of DED and LB-PBF processes

In this section, we contrast DED with that LB-PBF, which is the most popular metal AM technology investigated by far. Instead of feeding feedstock into melt pool continuously, LB-PBF spreads raw powders in a layer-wise manner. Compared to LB-PBF, DED is characterized by much higher building rate and its suitability to manufacture large blocks. The high building rate can be achieved due to the combined effect of feedstock and processing parameters, such as high heat source energy, large spot size, feeding rate, and layer height. Focusing on processing parameters, Table 1 provides a direct comparison of DED and LB-PBF processes [21, 38, 39, 41, 43-48, 50-59]. In DED process, large melt pools with widths ranging from 1500 to 3000 µm and depths of 500 to 2500 µm are created on the substrate surface with the laser spot size varying from 2 to 5 mm [67-69]. High heat source energy ranging from 200 to 5000 W (or arc current varying from 70 to 160 A) together with relatively low scanning speed (5-50 mm/s, which is two orders of magnitude lower than that of LB-PBF) provide the capacity to melt a mass of feedstock in short time, allowing for high feeding rate and therefore rapid manufacturing process. The resulted layer thickness is reported to range from about 0.3 to 2 mm [10, 63, 70], which is much higher than that of LB-PBF (limited to less than 100 µm [4, 6]).

In addition, DED process has been widely used for cladding and repair purposes for a very long time [61]. Recently, PFS is employed for process parameter optimization and part fabrication from a wide variety of materials, and through several innovative routes – to obtain superior mechanical properties. For instance, Kürnsteiner et. al [71] recently reported fabrication of superior Damascus steel-like parts of Fe19Ni5Ti containing periodic hard and soft layers generated by regulated cooling after every few layers. Similarly, Todaro et. al [72] employed high intensity ultrasound coupled with a powder based DED system to control the 3D printed microstructure of Ti6Al4V and achieve superior mechanical properties. The control of grain growth through ultrasound assisted agitation was possible due to absence of a powder bed in the DED process [73]. Moreover, given the negligible presence of powder feedstock inside the build chamber and that multiple hoppers can be attached to the powder inlet in experimental conditions, fabrication of a wide range of materials could be carried out with minimum housekeeping otherwise necessary in PBF processes when printing new alloy systems. As the blown powder is directed towards the melt pool for deposition and there is no need for a powder bed, the amount of feedstock necessary for part fabrication is greatly reduced. This is another advantage DED has over PBF processes when investigating AM of expensive alloy systems such as those with refractory elements. Table xx provides a comparison of the advantages and drawbacks of DED with respect to the other competing metal AM technologies.

- Microstructures of the DED-processed alloys

A few unique microstructural features are reported in DED components, which are different from that of CM counterparts. These differences arise from distinct thermal histories featured by high cooling rates (103 to 104 K/s) [28, 44, 74] and continuous thermal cycles in DED process, resulting in multi-scale, heterogeneous and hierarchical structures. In this section, formation and evolution of these common microstructural features are discussed.

  - Porosity

3.1.1 Nature and formation mechanisms of porosity

In both DED and LB-PBF metallic components, porosity is associated with the sub-optimum combination of the processing parameters and complex thermal history experienced by the solidification front, which is induced by focused and moving heat source [4, 44, 75-83]. Based on the mechanism of their formation, pores are categorized into lack-of-fusion (LoF) defects, gas and keyhole pores [4, 44, 75-83]. LoF defects are attributed to insufficient penetration of newly deposited layer into previous layers [75-77, 81]. As shown in Fig. 2a [84], they mostly occur along the layer boundaries and thus are commonly referred as interlayer porosity [77]. Irregular-shaped LoF defects with size of around 100 to 500 μm in equivalent diameter usually contain sharp corners [75-77, 81].  These defects are much larger than those identified in LB-PBF components (smaller than 200 µm) [85, 86]. Critical factors resulting in coarser LoF defects can be large melt pool size and layer thickness as shown in Table 1. Formation of LoF defects is usually accompanied by the appearance of partially molten powders due to insufficient heat input or high feedstock feeding rate [81].

The gas porosity in the DED components is primarily a result of the entrapped gases that fail to escape from melt pool before solidification. The sources of such gases are those within the original powders [44, 78], shielding gases [80, 82, 87], and vapors of the constituent alloying elements [75, 88]. Powders prepared through gas atomization may contain small gas pores filled with argon or nitrogen due to the gas entrapment [44, 78]. During DED process, shielding gases could be entrapped inside the melt pool because of the instability caused by the impact at melt pool surface [80]. Further, alloying constituent could vaporize due to very high temperature within the melt pool, producing high pressure bubbles and transforming into gas porosity [88]. The resulting pores are usually spherical due to internal gas pressure, see Fig. 2b [80].

Fig. 2c shows typical keyhole porosity [8] generated from the keyhole mode of melting [79, 83, 89]. Fluid flow dynamics within the melt pool can become unstable upon excess heat input accompanied by drastic fluid recirculation behind the keyhole, which results in rapid collapse of the keyhole and thus porosity [89]. Contrary to irregular-shaped LoF defects distributed along the layer boundaries, gas and keyhole porosities, also referred as intralayer pores [44], distribute randomly within the DED components [77, 81].

3.1.2 Strategies for porosity reduction

Complete elimination—if not, minimization—of porosity is absolutely essential in components that are susceptible to fatigue, as pores (especially those near or at the free surfaces) facilitate easy crack initiation and hence are highly detrimental to fatigue life of the component [4, 21, 75-77]. Since the raw materials used in metal AM are powders, most often, reduction/elimination of porosity is one of the inherent challenges for producing high-performance structural materials via AM. Although post-processing treatments, such as hot isostatic pressing (HIP) [83], can efficiently remedy this problem, these additional treatments will inevitably extend lead time and increase total cost of the component manufacturing, which impairs the dominant advantages of AM. Keeping this in view, several strategies that use either processing parameter optimization or powder characteristic control have been employed, which are summarized in this section.

As already mentioned, the unique thermal history associated with the AM processing plays a critical role in the development of porosity in the printed part. It is impractical to determine thermal history using a single parameter because of strong interplay among them. Currently, different models are proposed to describe thermal field related to processing variables, including volumetric energy density Ev [90, 91], linear heat input El [75, 92] and global energy density Eg [93], and normalized energy density En [94], which are defined as the following:

Ev=Pvwh																(1)

El=Pv                                                                                (2)

Eg=Pvd                                                                    (3)

En=Pvh.                                                                     (4)

In the above equations, P is the heat source energy, v is the beam scanning speed, w is the width of a single track, h is layer thickness, and d is the beam spot size. El could be suitable to predict formation of LoF defects since melt pool size is highly sensitive to P and v [95]. Increasing P can reduce LoF defects by enhancing melt pool size thus increasing the penetration depth that results in more compact interlayer bonding. In contrast, increasing v results in enhanced LoF defects due to reduced melt pool depth. Therefore, high El should be employed to avoid LoF defects. As shown in Fig. 3a, the monotonous reduction in the porosity volume fraction with increasing El in DED Inconel 718 alloy may be partially related to elimination of LoF defects [92].

While there is currently no consensus on a model that is most suitable to describe the relationship between processing parameters and intralayer porosity, it is generally agreed that excess heat input will lead to increased intralayer porosity [95, 96]. The steep and often complex thermal gradients associated with the DED process induce commensurate gradients in surface tension, which enhances the melt pool dynamics due to Marangoni convection [95-97]. By destabilizing the melt pool, which, in turn, could trap surface gases and do not allow the escape of inner gases, this aids in the formation of intralayer porosity [80, 95]. This is illustrated in Fig. 3b, wherein in situ x-ray imaging reveals that liquid melt driven by Marangoni convection folded over layer surface and entrapped gas bubbles [95]. Variation of the porosity as a function of Eg is plotted in Fig. 3c [93]. It shows a general trend that LoF defects decrease monotonously with increasing Eg, but the fraction of gas porosity increases after a critical value of Eg. By considering various processing variables and metallic materials, an optimal processing window for printing relatively dense parts, in which significant reduction or even elimination of porosity could be achieved, should exist. One practical method to contour (or at least narrow) the processing window of a given material is to conduct single track deposition studies and thin wall printing before block manufacturing [98].

Besides the processing parameters, the characteristics of the feed powders such as particle size, morphology [99], and initial porosity [81, 84] have substantial effects on the relative density of the as-printed parts. Powder-beam interactions in DED process are highly dynamic in comparison to the LB-PBF process. Consequently, the particle size determines its preheating as it moves across the beam and impinges the melt pool [100]. Spherical powders with less satellites that have high and stable flowability as well as ability to spread uniformly are highly desirable to fabricate dense blocks using DED. A comparison of single tracks deposited with identical parameters but different powder morphologies is made in Figs. 3d and e [99]. The relative densities of the DED components could be improved further by pre-heating the powders just before deposition, which removes the moisture and trapped gases, if any [99].

An inherent disadvantage of DED compared to LB-PBF is the lower relative density of the printed parts. While a relative density higher than 99.3 % (or even 99.8%) can be obtained using LB-PBF, it ranges from 99.0 to 99.5% in most DED components [76, 77, 85, 101, 102]. The difference in porosity level could be related to larger characteristic length scales in DED, such as powder size, melt pool size, layer thickness and resultant large pores.

  - Grain morphology

3.2.1 Columnar and equiaxed grains

The as-built (AB) DED alloys are composed of both columnar and equiaxed grains (see Fig. 4a for two kinds of grain morphologies in Ti alloys [26]). Compared to equiaxed grains, columnar grains are large and able to penetrate through several layers of deposited components. They originate from epitaxial growth of molten material from chosen substrate or previous layers. Such a growth is possible because the corresponding energy barrier is much lower than that for grain nucleation. Notably, certain growth directions are thermodynamically favored depending on the crystal structure of the deposited metals and alloys, which are referred as easy-growth directions and are listed in Table 2 [103]. Grains with easy-growth directions orienting closely to the direction of thermal gradient evolve into coarse columnar grains, while growth in other directions is suppressed, which is referred as competitive growth.

A competition between formation of columnar and equiaxed grains exists. Contrary to epitaxial growth, equiaxed grains develop because nucleation is thermodynamically and kinematically feasible through the process of either homogeneous nucleation upon constitutional undercooling or heterogeneous nucleation induced by partially melted feeding powders or by particles that are introduced deliberately as nucleants. The volume fraction φ of pre-formed equiaxed grains (or equiaxed grain embryos) during solidification can be determined using the equation [104]:

φ=1-exp⁡-4πN03(n+1)nGnaR3                                 (5)

where G is the temperature gradient, R is the solidification rate, and N0 is the number of nucleation sites. Equation 4 indicates that the combination of low G and high R together with the abundance of the nucleation sites could promote formation of randomly oriented equiaxed grains, which is illustrated by the solidification diagram in Fig. 4b [103]. The G/R ratio determines the mode of solidification, while the cooling rate T, given by G×R, dominates size of solidification structures. Hunt proposed that when φ is smaller than 0.66%, the newly formed equiaxed grains would be “swallowed” by liquid/solid interface driven by epitaxial growth, leading to fully columnar grains. When φ is larger than 49%, fully equiaxed grain structure is obtained as epitaxial growth is completely suppressed. For φ ranging between 49% and 0.66%, a mixed grain structure will be observed (Fig. 4c) [105].

One notably different feature between the columnar grains present in LB-PBF and DED components is that the columnar grains in the former are generally closely-oriented along the build direction [106, 107], while vertical, inclined, and even curved (zigzag-shaped) columnar grains are observed in the latter [108, 109]. Figs. 5 a-c show vertical columnar grains in LB-PBF Inconel 718 alloy (Fig. 5a [106]) and inclined (Fig. 5b) as well as curved (Fig. 5c) columnar grains in DED counterparts [109], which initiate and evolve as a result of the unidirectional and bidirectional scanning patterns, respectively. Key reason for such disparate grain structures is that melt pools with different morphologies form during LB-PBF and DED processes, i.e., small and shallow melt pool in LB-PBF [110, 111] while relatively large and deep melt pool in DED process [112, 113]. In LB-PBF, the melt pool boundaries are relatively flat with low curvature and the overall maximum heat flow direction is roughly parallel to the build direction, resulting in vertical columnar grains. In DED, however, the local curvature varies significantly and consecutively with different locations along the melt pool boundary. The superimposed effects of easy-growth direction and maximum heat flow direction give rise to straight but inclined columnar grains in DED that employs unidirectional scanning pattern. When a bidirectional scanning strategy is utilized, mirror symmetric melt pools are developed by the inverse scanning directions, resulting in periodical heat flow direction transformation and therefore zigzag-shaped columnar grains along adjacent layers.

3.2.2 Columnar to equiaxed transition (CET)

Long columnar grains could result in anisotropic mechanical behavior in metal AM parts [114, 115] and enhance susceptibility to hot cracking. Significant efforts have been made to explore strategies to enhance CET in DED components. As per equation (5), achieving low G/R by optimizing processing parameters is one practical method to promote CET. As shown in Fig. 6a, reduced laser power is demonstrated to enhance CET in the Ti5553 alloy [25]. In addition, increasing scanning speed contributes significantly to CET during welding (Fig. 6b) [116]. Numerical studies of laser assisted welding show that the regions with low G/R value in melt pool extend with increasing scanning speed [117]. Considering similarities between welding and DED processes in terms of thermal-physical properties, increasing scanning speed may also promote CET in DED components. Similar result was reported in the case of LB-PBF Inconel 718 [118], but this needs to be further validated for the DED process.

Increasing the powder feed rate can extend the equiaxed grain regions via the introduction of unmolten powders as grain nucleation sites [119]. However, this may also result in increased porosity. Alternatively, addition of micro/nano-scaled particles is proposed to help promote CET during AM processes. Studies focusing on Ti alloys reported that formation of large columnar grains could be suppressed through addition of either ceramic particles or solute elements (including TiC, TiB2, La2O3, B, Si, Co, Mo, Zr, etc.) [120-126]. Ceramic particles act as potent nucleation sites while the solute elements enhance constitutional undercooling. Therefore, both the methods are in fact aimed at enhancing equiaxed grain nucleation [120-125]. A typical work focusing on CET in Ti alloy following this strategy is shown in Fig. 6c, where grain structures of AB Ti-6Al-4V, Ti-3Al-6Cr-4Mo-4Zr and Ti-3Al-6Cr-4Mo-4Zr+La2O3 are presented from left to right [126]. Similar trends were identified in other alloys, like 316L SS [127] and Inconel 690 [128].

Although the addition of micro/nano-scale particles is proven to be effective in CET, the following factors need to be considered before its application. (i) For printing components with good structural integrity, suitable micro/nano-scaled particles for different engineering alloys need to be selected based on compatibility of crystallographic structures, lattice parameters, and thermal expansion. Non-compatibility can lead to internal stress generation, which, eventually, can impact the structural integrity of the component manufactured. (ii) Fabrication using raw feed powders that contain dispersed particles can be challenging, as micro/nano-scale particles tend to agglomerate due to high surface energy [129, 130]. (iii) Inhomogeneity in chemical composition and microstructural features induced by addition of the particles may also degrade other properties, especially fatigue and corrosion resistances [131, 132].

It is worth noting here that CET is not always beneficial to mechanical performance of components. For repairing of single-crystal or directionally solidified Ni-based superalloys using the DED technique, epitaxial growth is highly desired [133, 134] and CET will introduce stray grains and detrimental grain boundaries. In addition, the exploration of CET in components produced by AM should be judicious, because control over texture and morphology of grains gives an additional degree of freedom (from the microstructural design perspective) during AM process. This could be used to tailor the microstructure for enhancing properties in specific direction.

  - Cellular structures and dislocation network

3.3.1 Cellular structures

The metallic components fabricated using DED are frequently reported to contain solidification cellular structures [28, 29, 135-139], which serve as sub-grain structures embedded within individual grains. Figs. 7a and b show a 3D composite view and a SEM image of the cellular structures in DED 316L SS, respectively [28, 43]. Cells show straight columnar morphology approximately parallel to the build direction. When viewed from the top, they exhibit circular morphology and form dense networks. These structures are formed because of the constitutional undercooling that results from the elemental redistribution during solidification, which terminates planar growth and enhances cellular/dendritic growth. The equivalent diameter of the cells ranges from 1 to 10 μm [28, 29, 135-139]. It was demonstrated that cell boundaries are low angle grain boundaries (LAGBs) in nature with misorientation across two adjacent cells ranging from 1° to 4° (See Figs. 7c to e) [137]. The slight misorientation across adjacent cells is expected to be a combined effect of various factors, including thermal stresses caused by intercellular liquid solidification [137, 140] and complex heat flow fields [141]. It is important to note that not all metallic components manufactured using DED contain cellular structures; few examples are Ti alloys and some intermetallics [142-144].

The equivalent diameter of cellular structures in DED metallic components is about one order of magnitude larger than that of the cells in LB-PBF blocks (usually in submicron-scale size) [29, 55, 145]. Both experimental and simulation studies reveal that primary cellular arm spacing (PCAS, or cell spacing) is dominated by cooling rate T [43, 138, 146, 147]. The PCAS in AM components was observed to obey the relation [43]:

λ=80T-0.33.													(6)

T in DED process is determined to be 103 to 104 K/s [28, 44, 74], which is two to three orders of magnitude lower than that of LB-PBF process (105 to 106 K/s) [43, 145, 148]. The ultrahigh cooling rate in LB-PBF processing is primarily due to the combination of low heat source energy, high scanning speed, and small melt pool size (Table 1).

3.3.2 Elemental segregation and high density of dislocations

Several studies have reported of an overall elemental segregation in various DED-processed alloys [135, 136, 149, 150]. Fig. 8 shows an EDS map obtained on an AB 316L SS. It shows an enrichment of the cell boundaries with Cr, Mo, and Mn [135]. The reasons for such a segregation can be rationalized using the solidification theory. As solute elements usually exhibit higher solubility in liquid with equilibrium segregation coefficient smaller than 1, constituent elements with higher Tm are rejected from solid continuously during solidification process, piling up ahead of solid/liquid interface and resulting in constitutional undercooling.

High-density dislocations are another typical microstructural characteristic observed in DED-processed components. Fig. 9a shows transmission electron microscopy (TEM) images of the microstructures of DED 316L SS [151]. In most studies on DED alloys, these dislocations were reported to form networks similar to those observed in the samples subjected to low cycle fatigue loading [152] and LB-PBF alloys [153]. A low-density of homogeneously distributed dislocations in the interiors of the solidification cells were observed. In contrast, high-density tangled dislocations are observed to distribute along cell boundaries. It was suggested by Bertsch et al [149] and Li et al. [154] that the expansion/shrinkage strain cycles induced by the thermal cycles after solidification can be the key reason behind the high-density dislocations. Notably, TEM characterization by Li et al. reveals that these dislocations do not necessarily evolve into dislocation networks. Instead, they were observed to distribute homogeneously in AB 316L SS due to limited thermal cycles [154]. The dislocation densities reported in AB DED and LB-PBF alloys [136, 142, 149, 155-163] are listed in Table 3. Dislocation density in the former ranges from 1013 to 1014 m-2, which is considerably lower than those reported in the LB-PBF counterparts.

Besides the dislocation density, correlation between dislocation network and cell boundaries can be different in LB-PBF and DED components, manifesting as that dislocation network overlap with cell boundaries in LB-PBF components while distribute between cell boundaries in DED blocks (Fig. 9b) [149]. One critical factor that dominate the correlations of dislocation network and cell boundaries is the difference of size of cells and dislocation network [149]. Overlapping may break down when noteworthy difference exists between size of cells and dislocation network.

3.4 Microstructures in DED alloys

3.4.1 Steels

Alloys belong to the austinite SS grades are the most investigated DED alloys [23, 44, 135, 139, 164]. Fig. 10 shows the representative SEM and TEM images of typical microstructures in an austenitic (γ) 316L SS manufactured via DED [44]. Hierarchical microstructures resulting from far-from-equilibrium solidification process, with length scales ranging from nanometer to millimeter, can be seen in them [44]. The deposited sample is composed of millimeter-scale deposition layers, which are often termed as a ‘mesostructures,’ to distinguish them from the usual microstructure (Fig. 10a). Additional features are the micro-scale porosity, grains, and cellular structures (Figs. 10a and b), sub-micron-scale cell boundaries and dislocation networks (Figs. 10c and d). The melt pool boundaries seen in Fig. 10a form because of the rapid solidification that follows the continuous motion of heat source. The inhomogeneous temperature gradient distribution in the melt pool leads to a unique structure in DED 316L SS, manifesting as dominant epitaxial growth at melt pool boundaries but equiaxed grain nucleation in the interior of the melt pools [23]. Larger melt pools with lower cooling rates in DED 316L SS results in coarser grains compared to their LB-PBF counterparts. Ma et al reported that columnar grains in DED 316L SS are typically 50 to 100 μm in width and 500 to 2000 μm in length, which are much coarser than the columnar grains in LB-PBF 316L SS whose width and length range from 10 to 50 μm and 100 to 500 μm, respectively [43].

DED austenitic SSs usually have a small-fraction of the δ ferrite phase within the γ austenite matrix [23, 28, 44, 135], which is not present in CM counterparts and rarely observed in the LB-PBF counterparts. The volume fraction of the δ phase varies from about 1% to 11% and is sensitive to the solidification thermal history [23, 28, 44, 135]. The retained δ phase can be identified using XRD (Fig. 11a [135]), scanning transmission electron microscopy (STEM, Fig. 11b [135]) and electron backscatter diffraction (EBSD) (Fig. 11c [23]). The distinct XRD patterns of AB 316L SS blocks and initial powders (Fig. 11a) indicate that the δ phase forms during the solidification and does not pre-exist within the powders. A closer look (Fig. 11b) reveals that it preferentially occurs along the sub-grain and cell boundaries. This indicates that the appearance of δ phase is most likely related to micro segregation of δ stabilization elements (such as Cr and Mo) along the cell boundaries (Fig. 8) [135]. The underlying reasons for the absence of δ phase in LB-PBF 316L SS not well understood yet. We infer that one critical factor could be insufficient concentration of the δ stabilization elements along the cell boundaries in LB-PBF components due to smaller cell size and therefore higher volume fraction of cell boundaries [164, 165]. However, studies focusing on quantitative measurement of micro-segregation and solidification details are required. It should be noted that a homogenizing treatment at 1150 oC for 2 h can transform δ to γ completely as shown in Fig. 11c.

Precipitation hardening (PH) steels are another grade that are being increasingly adopted for AM [166-169]. Contrary to their wrought counterparts with fully martensitic phase in the microstructure [170], DED PH steels contain both martensite (M) phase as the matrix and retained austenite (γ phase) embedded in it [167-169]. The latter is a result of residual stresses built up due to high cooling rates and inherent cyclic thermal loadings. It is further chimerically stabilized by γ stabilizing elements due to micro-segregation [167-169]. The volume fraction of retained γ phase is sensitive to powder characteristics, processing parameters and deposition atmosphere [166, 167], i.e., enhanced retained γ content was identified in 17-4 PH steel manufactured in Ar atmosphere as shown in Fig. 12 [167]. The disparate printing variables lead to large scatter in the volume fractions of retained γ phase that are reported in several studies, which range from less than 10% to more than 50% [167-169]. Strategies on controlling the retained γ phase content could be developed based on available studies, i.e., air atmosphere chamber will substantially reduce retained austenite [167]. It is impractical to conduct quantitative comparison on volume fraction of retained γ phase in components manufactured via DED and LB-PBF, as even larger scatter in volume fraction (from less than 1% to more than 80%) is reported in LB-PBF components [171-174]. Furthermore, smaller grains in the LB-PBF 17-4 PH steel inhibit austenite to martensite transition and are partially responsible for the γ phase dominant microstructure [167].

For the AM 17-4 PH steel, heat treatment (HT) after deposition is required to precipitate the Cu-rich particles and transform the retained γ to M phase, which imparts high strength to the components [167, 170]. The conventional HT consists of solution treatment (ST) and subsequent aging treatment (AT) [167]. Retained γ phase are reported to deteriorate strength of the alloy due to the higher solubility of precipitate elements in austenite. Thus, a preliminary ST that transforms γ into M is imperative to produce high-strength PH steels [167, 171]. Notably, initial retained γ may not totally transform into M through HT conducted at low temperature or with short time, which is attributed to a few factors, including the elemental segregation that leads to γ stabilization, nitrogen, finer microstructural sizes, and residual stress [164, 167].

3.4.2 Ti alloys

The Ti-6Al-4V alloy is one of most thoroughly researched Ti alloy for AM due to its wide range of application potential [47, 114, 175-181]. Within the columnar prior β grains, both acicular α' martensitic phase [181] and lamellar α+β phases in the form of either basketweave Widmanstätten [179] or colony structures [47] were reported in the AB DED Ti-6Al-4V components (Fig. 13a-c). This is in contrast to the microstructures dominated by α' in most AB LB-PBF Ti-6Al-4V [148, 182-185]. The microstructural phases in the AB DED Ti-6Al-4V are highly sensitive to the cooling rate, which is affected by the process parameters and the build geometry used [47, 178-181, 186, 187]. While a high cooling rate during solidification results in the presence of acicular α' phase, lamellar α+β phase appears in regions that experience relatively lower cooling rates. In the latter case, the lath thickness increases with reduced cooling rate. In CM Ti-6Al-4V, the critical cooling rate above which acicular, long orthogonally oriented α' phase forms was determined to be 410 oC/s [188]. However, a critical value of 4344 oC/s, which is one order of magnitude higher than that determined for CM of Ti-6Al-4V, is reported for DED Ti-6Al-4V, shown as sharp reduction in volume fraction of the α phase above the critical value (Fig. 13d) [74]. This value should be reasonable considering typical cooling rates and phase compositions in DED Ti-6Al-4V. We infer the key factors, which result in this sharp difference in critical temperatures in CM and DED components, can be the residual stress and elemental segregation during DED, but more quantitive experimental and modeling studies are required. In addition, potential phase transformation after solidification upon cyclic thermal loading may also influence the evaluation of the critical cooling rate [16].

Gradations in the phase fractions, as a result of the different cooling rates along the build direction, were reported by Brandl et al in DED Ti-6Al-4V [47]. Martensite α' phase appears in the first few layers near substrate due to highest cooling rate in this region. With an increase in the build height, lamellar α+β phase starts appearing as a result of reduced cooling rate [47]. Components consisting dominant martensite α' phase could also be manufactured via DED with low laser energy; a microstructural transition from α' phase to mixed phases (α' and α) is reported when the laser energy is increased from 330 to 780 W [180]. As shown in Fig. 13e, α is observed along the prior β grain boundaries [114]. Ahmed et al proposed that such grain boundary α forms when the cooling rates are lower than that required for the α' phase formation but are higher than that required for the lamellar α+β phase formation [188]. From the application stand-point of view, an alloy containing the martensitic α' microstructure is not favored because of its relatively brittle nature compared to the once containing the α+β phases. The adverse effects of acicular α' phase can be eliminated through decomposition of α' phase into a mixture of α + β through the post-processing HTs [178]. HT below the β-transus temperature (Tβ) is preferred because exposure to higher temperature can excessively coarsen the microstructures.

Apart from post-processing HT, decomposition of acicular α' could also be triggered by in situ HT from the cyclic reheating [16]. As shown in Fig. 13f, phases vary across the layers in Ti-6Al-4V depending on their exposure to thermal cycling. Since the top layers undergo only a few thermal cycles, either α' or α+β phases (depending on cooling rate) dominate the microstructure. As for layers in middle region, original phase transforms into β phase when the peak temperature is higher than Tβ and subsequently transform into either α or α' phase upon cooling [16]. For even lower regions, the peak temperature is below Tβ and phase coarsening, instead of phase transformation, happens upon thermal cycling. Thus, Fig. 13f provides an approximate depiction of the phase evolution do the varying thermal cycles experienced at different build thickness’. However, there might be deviations, to some extent, due to variation in processing parameters, scanning strategy, and resultant thermal history.

3.4.3 Ni-based alloys

Ni-based alloys are another group materials that have attracted tremendous interest for DED. Among them, Inconel 625 and 718 superalloys were the most studied to date [17, 35, 189-198]. Figs. 14a and b show the grains and phases in AB DED Inconel 718 alloy [196]. The resistance to deformation at high temperature in Ni-based superalloys mainly originates from the γ’’ and γ’ precipitates. However, γ’’ and γ’ phases are usually absent [35, 196, 197] or very low volume fraction of them has been reported in the AB condition [91, 194] as the inherent high cooling rates of DED prevent their precipitation [197]. However, this may not be the only reason, because γ’’ phase was observed in the LB-PBF Inconel 718 alloy that experiences even higher cooling rates [52]. Factors, such as dissolution of γ’’ and γ’ phases upon thermal cycling, depletion of elements due to elemental segregation, and formation of other precipitates, could also play critical roles in this context. Alloying element Nb was reported to segregate along the cellular boundaries and enhance formation of the Laves phase in AB Inconel 718 alloy, as shown in Fig. 14b [196]. Tian et al also reported the appearance of Nb-rich eutectic structures containing Laves phase and MC carbides (mostly NbC) in DED Inconel 718 alloy [193].

The absence (or very low volume fraction) of γ’’ and γ’ phase combined with the prevalence of irregular shaped Laves phase make it impractical for AM Inconel 718 superalloy to be employed directly in the AB condition without a post-processing HT [196, 197]. Typical HT consists of optional homogenization treatment at around 1080 °C for 1 to 2 h, followed by ST at 980 °C for 1 to 2 h, double AT at 720 °C for 8 h and 620 °C for 8 h, respectively [92, 190, 196-198]. Figs. 14c to h show the grains and main phases in DED Inconel 718 alloy in the ST+AT (SAT) and homogenized+ST+AT (HSAT) conditions [196]. Here, the temperatures used for AT are not high enough to dissolve the Laves phase completely (Fig. 14d). Therefore, ST at a higher temperature is a prerequisite to eliminate them and release the Nb for subsequent precipitation of γ’’ and γ’ phases. After incorporating ST, fine γ’’ and γ’ phases form abundantly in Inconel 718 alloy after both STA and HSTA. Notably, ST at 980 °C was reported to result in local Nb-rich regions and formation of δ phase with high critical solvus temperature (about 1010 °C) [196]. In addition, residual Laves phase was identified in LB-PBF Inconel 718 after ST at 980 °C for 1 h [199]. Thus, preliminary homogenization treatment is preferred for achieving higher γ’’ and γ’ phase contents.

Both experimental and simulation studies found that the formation of the Laves phase in Inconel 718 alloy is sensitive to the solidification structures that are dominated by G and R during the DED process [200, 201]. Small equiaxed dendrite arm spacing resulting from a low G/R ratio leads to discrete Laves particles. In contrast, large columnar dendrite arm spacing, originating from a high G/R ratio, results in continuous and coarse Laves particle networks. Therefore, the morphology of Laves could be regulated for a reduced hot cracking susceptibility through the optimization of the processing parameters, such as increasing laser energy and reducing scanning speed.

- Mechanical properties

In this section, uniaxial tensile and fatigue properties of DED components are summarized with special emphasis on relationships between processing parameters, microstructures, and properties.

  - Uniaxial tensile properties

4.1.1 Overview

In general, the tensile strength of the DED alloys is either comparable or superior to that of their CM counterparts. Although grains in them are usually large (tens to even hundreds of micrometers [16, 43]) and thus not expected to result in high strength based on the Hall-Patch relation, some other factors, including a high-density of dislocations, elemental micro-segregation, and dispersed particles, contribute significantly to the strength as discussed below [136]. However, their strength is relatively inferior compared to that of the LB-PBF counterparts. This is not only due to larger grain size in DED alloys but also coarser sub-grain features as well as lower initial dislocation density (Table 3) [43, 114, 139, 180].

A large scatter in the reported ductility values, regardless of the alloy, is common. The observed scatter originates from discrepancy in structures (porosities, phases, and grains) in the same alloy resulted from different thermal histories due to various processing parameters and build geometries. For instance, much higher ductility is reported in AB Ti-6Al-4V consisting of α+β phase than that containing intrinsically brittle martensite α’ phase [178, 179].

Another feature that distinguishes DED components from CM counterparts is the anisotropy in tensile properties, which can be attributed to a combined effect of various factors, such as columnar grains and LoF defects [16, 114, 178, 179]. Tensile strength and ductility are sensitive to the loading direction with respect to the build direction, making it imperative to conduct mechanical tests along different orientations to gain a comprehensive understanding of tensile properties of DED components.

4.1.2 Strengthening in DED components

The strengthening mechanisms that are commonly observed in the DED alloys are similar to those observed in their CM counterparts [154, 202, 203]. However, the superior strength of the former vis-à-vis CM alloy of the same composition cannot be rationalized by the grain boundary and precipitation strengthening mechanisms due to coarse grain size and precipitate spacing [16, 28, 29, 43]. Instead, the existence of dislocations in high densities in the AB condition itself and the prevalence of their networks plays a dominant role. This is verified by the sharp decrease in hardness upon high-temperature annealing in DED 304L SS [204]. Although the dislocation density could vary with the location in a DED component (reported to decrease with increasing distance from baseplate along build direction [136]), initial high dislocation densities, ranging from 1013 to 1014 m-2, result in significant forest strengthening [136, 142, 158]. Smith et al reported that dislocations at the level of 1013 m-2 results in strengthening as high as 166-191 MPa, which accounts for a large fraction of σY in DED 304L SS [136]. The strengthening was, to a certain extent, underestimated as dislocation density used here is density of GNDs, instead of density of overall dislocations. Additional strengthening is provided by elemental segregation along cell boundaries. Coherent internal stress induced by the chemical misfit in element enriched regions could restrict dislocation mobility and could contribute to the observed high strength [205].

In many studies, the cell boundaries are simply treated as conventional HAGBs and the classical Hall-Patch relation is then used to estimate the strengthening caused by them by using cell size as the characteristic microstructural length scale (instead of the grain size) [145, 206]. However, the misorientation across two adjacent cells is very low [137]. Therefore, they might not act exactly the same way a HAGB would in resisting the dislocation motion. This deduction is verified by results showing that σY calculated using cell size following Hall-Patch relation is higher than experimental value in LB-PBF high entropy alloy [207]. Li et al reported that initial dislocation density, instead of cell size, dominated the σY of small-volume pillars [208]. For DED components, strengthening related to cellular structures can be more complicated regarding that dislocation network may not always overlap with cells [149]. Thus, one critical issue needed to be addressed is which factor (cells or dislocation network) plays a dominant role with regards to strengthening. Although in situ experiment revealed that dislocation network could hinder but not completely stop dislocation motion under straining [209], overlapping of cells and dislocation network in LB-PBF 316L SS makes it biased to draw a conclusion on this issue. The elemental segregation along cell boundaries further makes it challenging to explore related strengthening. Thus, comparative study on materials with different cellular structures and dislocation networks may help shed light on effects of these two factors.

4.1.3 Steels

We first focus on the properties of DED austinitic stainless steels. Their tensile properties, i.e., σY, ultimate tensile strength (UTS, σUTS) and elongation to failure (εf) of DED-processed 316L and 304L SSs that are reported in the published literature are summarized in Table 4 [23, 28, 29, 135, 136, 210-215]. The horizontal and vertical directions here represent directions perpendicular and parallel to the build direction, respectively. Majority of these studies show that both these alloys exhibited superior σY, comparable σUTS but inferior ductility relative to their CM counterparts. The variability in the reported tensile properties of 316L SS is considerable with σY, σUTS and εf ranging between 270 and 580, 430 and 710 MPa, and 13% and 60%, respectively. Such a large scatter may be associated with a few factors including powder characteristics, the type of equipment employed for DED, processing parameters, and build geometries. It is important to note here that the tensile properties could vary from location to location within one single built block due to the gradation in the microstructures as well as residual stressed that develop because of the varying thermal histories experienced. Usually specimens extracted from the top show lower σUTS compared to those from the bottom because of coarse microstructures and lower dislocation densities arising from reduced cooling rate in the former [136, 215].

Figs. 15a to c compare σY, σUTS and εf of DED 316L SS with the respective properties of wrought alloy [23, 28, 29, 135, 145, 210-214]. In the DED alloy, the difference between σY and σUTS is relatively smaller compared to that in the wrought one, indicating that the former do not strain harden as much as the wrought alloy. Li et al. have shown that this behavior is directly linked to the      The limited strain hardening could be one of the reasons behind reduced ductility, and other factors would be the presence of processing-inherent flaws (especially LoF defects), brittle phases, and inclusions (mainly oxides) in the microstructure of the printed alloy. For instance, defect-driven failure featured by bifurcating cracks originating from irregular shaped pores was reported in LB-PBF 316L SS [216]. Since the DED parts contain even larger LoF defects, they could lead to lower ef. Apart from these factors, ductility diminishes dramatically (by over 50%) when oxygen content increases from 642 to 3710 ppm [28]. A comparison of the tensile properties of AB DED [23, 28, 29, 135, 210, 211] and LB-PBF 316L SS [214, 217-219] is made in Fig. 15d in terms of a σY vs. εf plot. As seen from it, DED 316L SS has a relatively lower strength but higher ductility, which is well expected considering relatively coarser microstructure and lower dislocation density (Table 3) in it in the AB condition.

Anisotropy in tensile properties is evident in both 316L and 304L SS produced by DED. The anisotropy index A defined as [187],

A=σl-σtσl×100%                      (6)

can be used to capture it quantitatively. In the above equation σl and σt are tensile properties (σY, σUTS or εf) along horizontal and vertical directions, respectively. 316L and 304L SS show relatively higher σY and σUTS when in the horizontal orientation, which is indicated by positive anisotropy index (anisotropy in yield strength, AY), as seen from the data provided in Table 4. In contrast, an opposite trend is observed in εf, which shows a negative anisotropy index (anisotropy in elongation, Aε). The observed anisotropy in tensile strength can be attributed to the combined effects of unique solidification microstructures (such as columnar grains and crystallin texture) and manufacturing deficiencies (such as LoF defects) [115]. For instance, when the long axis of the LoF defects is oriented approximately perpendicular to the build direction, they can susceptible to easy crack initiation under loading along vertical direction, but tend to close upon loading along horizontal direction [173].

Table 4 shows that AB 17-4 PH steel has significantly lower strength compared to their HT counterparts. This is due to the presence of soft austenite phase and absence of Cu-rich precipitates in the AB condition [167, 168, 220, 221]. Post-processing HT that promotes transformation of retained austenite to martensite and introduces Cu-rich precipitates in the matrix could significantly improve strength, but at the expense of ductility (Table 4) [164, 167, 220]. Caballero et al reported that microstructure containing nearly 100% lath martensite could be obtained through ST at 1040 °C for 0.5 h, but the alloy’s tensile strength is still relatively low due to the absence of precipitates. Comparable strength in AB and ST 17-4 PH alloys was reported due to superimposed effect of softening induced by annihilation of initial dislocations as well as elemental segregation and hardening originating from phase transformation in the former [220]. Only components subjected to ST followed by AT with considerable strength and ductility meet the requirements for practical applications [220]. In addition, transformation from retained austenite to martensite induced by plastic strain was reported in LB-PBF AB 17-4 PH steel, which gave rise to considerable ductility (around 50%) and high σUTS [222]. However, the possibility of such a transformation occurring in the DED 17-4 PH steel is not examined yet. The alloy’s relatively low ductility indicates that such transformation may not be easily achievable in it.

With the available data, no conclusion can be drawn regarding the tensile anisotropy of DED-processed 17-4 PH steel because of the scatter in the limited data (Table 4). However, studies indicate that it may be eliminated through ST followed by AT, which has been ascribed to the elimination of columnar grains due to recrystallization and formation of Cu-rich precipitates.

4.1.4 Ti alloys

Tensile properties of DED Ti-6Al-4V alloy in both AB and HT conditions are summarized in Table 5 and compared to those of its wrought counterpart [16, 114, 178-180, 223-226]. Majority of studies show that tensile strength of DED Ti-6Al-4V is comparable or even superior to that of wrought counterpart. σY and σUTS of AB Ti-6Al-4V range between 800 and 1100 MPa and 1000 and 1150 MPa, respectively. The σY versus εf plot for both DED and LB-PBF Ti-6Al-4V in the AB condition displayed in Fig. 16a shows that the DED alloy is featured by lower strength but significantly higher ductility, similar to that seen for 316L SS [114, 148, 178-180, 182-185, 223-225]. The striking difference in mechanical properties of LB-PBF and DED Ti-6Al-4V is a result of the disparate microstructures developed in them due to vastly differing cooling rates. As mentioned already, the microstructures of most AB LB-PBF Ti-6Al-4V are dominated by the α’ phase, which is hard [148, 182-185], while majority of AB DED Ti-6Al-4V consist of softer but ductile α + β microstructure (Table 5) due to relatively lower cooling rates [114, 178-180, 223-225]. The strength of Ti alloys consisting of lamellar α + β structures is expected to be dependent on thickness of α lath following the Hall-Patch relation, and α lath is usually thinner than 2 μm in AB DED Ti-6Al-4V [179, 180].

The ductility of AB Ti-6Al-4V alloys reported in some studies cannot meet the minimum value recommended for use in structural applications (Table 5) [178, 180, 223]. Post-processing HT could be a practical method to improve ductility by regulating the microstructures in terms of either α lath coarsening [224] or phase transformation from α’ to α + β [178] (Figs. 16 b and c). Notably, enhancement in ductility through HT is achieved at the expense of strength. Thus, it is important to choose proper HT parameters (temperature, hold time, and cooling rate) to achieve desired combination of strength and ductility for specific applications. Besides post-processing HT, in situ HT could be a more direct way to obtain required microstructures [16]. The difficulty in employing this method lies in the nonlinear interactions among various processing variables and resultant difficulty in achieving accurate control on the thermal cycles experienced by the alloy. Knowledge gained from detailed simulations using the existing experimental data could aid in the design of an optimum in situ HT for different component geometries.

Besides fine α lath and α’ phases, the ductility of Ti-6Al-4V is also influenced by some other factors, including grain boundary α (Table 5) and process related attributes, i.e., porosity and residual stresses [4, 114, 178, 180, 227]. The combined effects of these factors are responsible for the observed large scatter in εf.

Values of σY, σUTS and εf along horizontal direction of the DED Ti-6Al-4V are plotted against the respective properties that are obtained along the vertical direction in Figs. 16d and e. The anisotropy in σY and σUTS is only minor, with the strength values in the horizontal direction being higher by 5-10%. As indicated by both positive and negative values of Aε listed in Table 5, no clear trend in the anisotropy in ductility of the AB Ti-6Al-4V alloy. This is most likely due to combined effects of discontinuous α phase along prior columnar β grains and LoF defects in Ti-6Al-4V [114].

4.1.5 Ni-based alloys

The strength and εf values of DED Inconel 718 alloy in both AB and HT conditions reported in literature are summarized in Table 6 [92, 190, 196, 198, 228-232]. In the AB condition, σY and σUTS range between 600 and 700 MPa and 850 and 1000MPa, respectively. These are inferior to the respective properties of the wrought alloy [233]. The much lower strength is due to the absence of γ’’ and γ’ phases in the AB conditions. Fig. 17a plots σY versus εf of AB DED Inconel 718 [196, 198, 228-231], in comparison with AB LB-PBF counterpart [53, 199, 234-238]. Similarly, LB-PBF Inconel 718 shows higher strength but lower ductility, which is likely due to finer structures.

As pointed out previously, SAT and HSAT elevate σY and σUTS of Inconel 718 to 1000-1259 MPa and 1200-1450 MPa, respectively. Although the available data is somewhat scattered, σY and σUTS of DED Inconel 718 after HT are similar to those of their wrought counterparts [198]. Following typical strength-ductility trade-off in metallic materials, enhancement in strength via HT inevitably results in reduced ductility, but majority of studies report εf ranging from 10% to 20%, which is again comparable or superior to the ductility of the wrought counterparts [198]. The favorable combination of strength and ductility of the DED alloy originates from dissolution of Laves phase and precipitation of fine and uniform γ’’ and γ’ phases upon HT [92, 196, 198, 232]. Fig. 17b compares the strength and εf of DED [92, 196, 198, 232] and LB-PBF [53, 199, 234, 237] Inconel 718 in the HT condition (HT here is either SAT or HSAT). It appears that LB-PBF Inconel 718 has better combination of strength and ductility, manifesting as comparable εf but higher strength. The is a result of the combined effect of the following factors. (i) Relatively smaller and more homogeneous γ’’ and γ’ phases after HT [196, 238]. (ii) Smaller retained grains after STA. (iii) Higher relative density with lower porosity [198].

There are not enough experimental data to determine anisotropy in tensile properties of DED Ni-based alloys. For DED Inconel 718 without HSAT, columnar grains are dominant and expected to result in anisotropy in mechanical performance [196, 198]. However, presence of intermetallic (such as Laves phase) along inter-dendritic regions and grain boundaries may make the anisotropy less predictable. After HSAT, much weaker anisotropy can be expected due to equiaxed gains that result from recrystallization together with uniformly distributed precipitates [196, 198].

  - Fatigue behavior

4.2.1 Overview

A key aspect related to the structural integrity of metallic components is their resistance to failure under cyclic loading conditions. It becomes even more important for parts produced by AM, considering the presence of defects and very high surface roughness in the AB condition. Studies focusing on the fatigue behavior of AM components have been performed on a variety of alloys [195, 239-243]. In low cycle fatigue (LCF) regime, fatigue life of DED components can be either superior or inferior to their wrought counterparts, depending on the testing modes [244]. For example, the higher strength of  DED Ti-6Al-4V vis-à-vis the wrought alloy results in enhanced fatigue life under high cycle fatigue (HCF) conditions, but reduced low cycle fatigue (LCF) life due to low ductility [244]. In the HCF regime, defects and high surface roughness inherent to layer-wise manufacturing method result in inferior fatigue behavior [195, 243-245]. A typical example is shown in Fig. 18 providing comparison between fatigue behaviors of wrought and DED Ti-6Al-4V alloys in both AB and HT conditions [244].

4.2.2 Effects of porosity

The inevitable presence of porosity in most AM components in the AB condition is one of the main factors that deteriorates their fatigue performance. Pores can significantly reduce the cycles required to initiate the fatigue crack in the ‘total life’ approach of fatigue life assessment and results in premature failure [246-248]. The extent to which porosity is detrimental to the fatigue behavior is influenced by the pores’ size, morphology, and location. Generally, large irregular-shaped LoF defects with sharp corners located on or just beneath free surface reduce fatigue life to the largest extent due to markedly high stress concentration they cause [246-248]. Liu et al [249] reported that the fatigue life increased monotonously with increasing distance of the crack-initiating pores to the surface in a DED Ti alloy, while the variation of fatigue life with the pore size is less regular. It can be inferred that once the defect size exceeds a critical value, the spacing between defects and the free surface, instead of the defect size, dominates the fatigue life of AM components. Fig. 19 presents the fatigue fracture morphologies of DED Ti-6Al-4V [244] and Inconel 718 alloys [195], showing that pores serve as the preferential crack initiation sites under cyclic loading. Reducing porosity through process parameter optimization can improve the fatigue strength. For example, near-full density DED Ti-6Al-4V samples shows HCF strength of about 477 MPa, which is three times higher than that with measurable porosity [250].

The differences in the pore features of LB-PBF and DED components lead to dissimilar fatigue resistances; DED alloys’ fatigue behavior is generally inferior [195, 244, 251-253]. For example, fatigue strength of the LB-PBF Ti-6Al-V alloy in the AB condition was reported to range from 340 to 475 MPa [251], which is significantly higher than 254 MPa measured in DED Ti-6Al-4V [244]. It is proposed that there exists a critical size for porosity in Ti-6Al-4V, above which porosity substantially deteriorate fatigue properties [251]. As DED components are featured by inherently lower relative density and larger porosity size in comparison with LB-PBF counterparts (i.e., below 99.5% versus above 99.3% for relative density and about 100-500 μm versus below 200 μm for LoF defect size) [75-77, 81, 85], the possibility of finding pores near the free surface with size exceeding the critical value can be much higher in DED components, resulting in inferior fatigue performance.

It is worth noting that the influence of these pre-existing porosity on the LCF and HCF performance are quite different due to distinct fatigue damage evolution processes in the respective regimes [242]. In LCF, fatigue crack propagation dominates the fatigue life and easy crack initiation from the pores is expected to slightly deteriorate LCF performance. This was verified by the fact that LCF fatigue life decreases marginally with the existence of a small surface defect in Ti-6Al-4V samples [239, 248]. As for the HCF regime, the fatigue performance is mainly dependent on crack initiation and porosity leads to significantly reduced fatigue resistance by accelerating it [195, 239]. Furthermore, AM components with higher ductility deliver relatively lower sensitivity to dispersed defects. This is ascribed to the localized plastic deformation zones that form surrounding these defects, which blunt the stress concentrators and, in turn, enhance the tolerance to localized fatigue damage [254].

4.2.2 Effects of surface roughness

High surface roughness (Ra) is another main drawback of AM (Table 1), which provides stress concentrators under cyclic loading and deteriorates fatigue behavior like porosity. However, most of the work focusing on effects of Ra on fatigue behavior reported thus far was conducted on LB-PBF components [255-258] and few studies explored this topic in DED components. These studies show that reducing Ra through post-processing machining and/or polishing could substantially improve fatigue performance of AM components, especially in the HCF regime [255-258]. This is likely to be the scenario in the case for the DED components as well. Since Ra of DED components is either comparable to or higher than that of LB-PBF components (Table 1), post-processing machining become mandatory for parts that experience cyclic loading in service, especially those manufactured via WFS.

It should be noted that available studies focusing on fatigue behaviors of DED components are quite scarce (especially in the HCF regime) and far from adequate in providing a comprehensive description on this topic. Although considerable fatigue database was developed in the field of LB-PBF, the dissimilar features in LB-PBF and DED components in terms of characteristic scale, phase composition and residual stress make it challenging to extrapolate fatigue performance of DED components based on available data. In this context, more studies focusing on the fatigue properties DED alloys and components are required, which will help guide design of mechanically robust DED components.

- Unique applications of DED technique

5.1 Fabrication of graded materials (GMs) using DED

Compared to other manufacturing methods, DED is demonstrated to be ideally suitable to produce GMs that are usually employed in complex conditions where component properties are required to vary with the location [12, 259-263]. Equipped with two or more powder hoppers, DED systems deposit customized GMs by varying the volumetric/weight fractions of each constituent stock fed to the melt pool [264, 265]. Current studies mainly employ alloys with the detailed knowledge base in AM filed (such as austenite SSs, Ti alloys and Ni-based superalloys) [260-269], elemental powders [270] and ceramic powders [271-273] as the feed stock.

Presently two types of fabrication methods are popular for building GMs using DED. In one case, the fabricated GMs consist of metallic matrix with gradation in the ceramic particle reinforcements with maximum volume fraction not exceeding 50% along the build direction [271-273]. In the second case, GMs are fabricated by combining two different kinds of metals/alloys, i.e., mixed metals/alloys with a graded composition in the intermediate region and 100% composition at both ends [260-270]. A typical example of first type of GMs is shown in Fig. 20a, where crack-free TiC-reinforced Ti-6Al-4V GM with TiC increasing 1 vol.% along adjacent layers till reaching a maximum of 50 vol.% was fabricated [271]. Mechanical tests showed that although hardness improved monotonically with increasing TiC composition, tensile strength reached its maximum value with 5 vol.% addition of TiC particles and then decreased sharply due to premature failure [271]. Similar enhancement resulted from addition of TiC were reported in other Ti-based GMs [272, 273].

Ti and Ti-based alloys were joined with other metals/alloys to form the second type GMs [268, 269]. In the Ti-6Al-4V/Ti-6.5Al-3.5Mo-1.5Zr-0.3Si GM, the addition of the latter constituent leads to thinner α laths accompanied by an increased volume fraction of the β phase [266]. Similar phenomenon is observed in graded Ti/V and Ti/Mo deposits [270]. Apart from these, some other alloys were employed to fabricate GMs. As shown in Figs. 20b and c, a total of 24 layers consisting of 304L SS and Inconel 625 alloys with graded volumetric fractions in consecutive layers were deposited in the graded region via DED [267]. Consequently, microstructural gradation also develops in the fabricated GM. Their features are highly sensitive to the changes in the local composition. For instance, a transition from cellular to columnar dendrites happens with increasing Inconel 625 [267]. However, mechanical properties of such GMs are challenging to be predicted currently, manifesting as irregular/unpredictable property evolution along with composition gradient. Fig. 20d shows that hardness first decreases with the addition of Inconel 625, followed by a continuous increase and reaches the level of deposited Inconel 625 at a composition of 47 wt.% 304L SS [267]. In the Ti/V and Ti/Mo GMs, however, the micro-hardness increases first and then decreases with a continuous increase in the V/Mo contents along deposited samples [270]. Such irregular variation in the mechanical properties in the gradient regions is due to not only the compositional changes, but also process-induced microstructural variation in terms of grain size, grain morphology, and so on.

One major drawback of GMs produced using DED is their higher susceptibility for cracking, which is related to the formation of undesirable intermetallic phases, such as carbides in 304L SS/Inconel 625 [267], σ-FeV and BCC (Fe, V) solid solution phases in 304L SS/V/Ti-6Al-4V [268], and FeTi and Fe2Ti in Ti-6Al-4V/Invar [269]. Figs. 21a and b show fractured Ti-6Al-4V/Invar GM due to cracking [269] and a tortuous crack path within the 304L SS/Inconel 625 GM [267]. Efforts have been made to mitigate or eliminate cracking in GMs by exploring the thermodynamics related to the evolution of various intermetallic phases during DED [265]. A precise control on the composition of different contents provides the opportunity of evaluating intermetallic phases using the phase diagrams [267]. For example, the predicted phase evolution as a function of the composition and temperature in the 304L SS/Inconel 625 GM is shown in Fig. 21c [267]. In many cases, intermetallic phases inevitably appear when linear combinations of two component powders are used. This is due to the large formation window. In this context, the gradient paths, which go through gradual transition from one constituent to the other, could be chosen alternatively. Fig. 21d demonstrates three typical gradient paths that are available within the Ti6Al4V/V GM with a fixed Ti/Al ratio at 750 °C [265]. Path 1 employs component powders with fixed element ratio. Path 3, instead, adopts elemental (Ti, Al, and V) powders and is capable to tune atomic ratio of all elements randomly, which dramatically improves the compositional freedom and, in turn, microstructure, and property design. However, producing GMs through path 3 is costly due to the high production cost of elemental powders. In addition, it can be challenging to acquire a precise control on elements with marginal content using path 3. Fabrication ofFGMs using DED is still under exploration and a comprehensive understanding of composition interactions and phase evolution is critical to manufacture GMs with the desired properties.

5.2 Component repair using DED

DED is a promising method to repair high value components which are difficult or costly to be replaced [13, 14, 274-281], such as gas turbine blades consisting of directionally solidified or single-crystal Ni-based superalloys. One practical example is that of a damaged gas turbine compressor seal repaired by depositing Inconel 718 alloy at a cost of 45% of new component [282]. Component repair using DED involves the injection of the feedstock into melt pool at specific locations (that require repair) guided by a digital model that is determined by the difference between 3D models of original and damaged components [280]. Figs. 22a and b show images of damaged turbine blade before and after repair, respectively [281]. In the repair process, compact metallurgical bonding is required between the deposited material and base substrate without losing the integrity of the components [278, 281]. In addition, both the component’s geometry and mechanical properties are required to be restored by the repair procedure. The flexibility inherent to DED makes it ideal for restoring the geometry. Restoration of the mechanical performance to the pristine levels, however, can be challenging due to limited control on the microstructure evolution, including grain features, phase compositions, and elemental distributions. Oh et al reported that compact bonding could be achieved between deposits and damaged substrates in both CM and LB-PBF 316L SS (Fig. 22c) [278]. In addition, tensile properties of the above two components with shallow grooves could be completely restored after repairing them with DED. Table 7 provides a comparison of the mechanical properties of various alloys in undamaged and repaired conditions [13, 278, 281]. While the tensile properties of some repaired components are comparable to their undamaged counterparts, the others show inferior mechanical performance due to cracking and oxidization [278]. Additionally, martensite formation in the DED layers of AISI 4340 steel, due to the relatively rapid cooling, results in hardness enhancement at the cost of ductility and toughness, and therefore post-repair HT is required [283]. Above studies indicate that some issues exist in achieving restoration of both geometry and mechanical property through DED and further investigation is required to enhance the understanding of this emerging process.

During the repair of components with singe-crystal grain or directionally solidified grains using DED, stray grains with considerable misorientation from adjacent grains can frequently form [284, 285]. The principles guiding repair of such components is to maintain the epitaxial growth from baseplate and prevent the nucleation and growth of equiaxed grains. Going back to Section 3.2, a combination of high G, low R and limited N0 is favorable for this. Thus, the formation of stray grains could be suppressed by adopting optimized combination of process variables, such as low substrate temperature, reduced laser beam energy, and low laser beam size [104]. Notably, the melt pool morphology needs to be considered specifically for DED-repair process. Stray grains were reported to form along the melt pool boundary with large curvature due to considerable misorientation between heat flow direction and preferred growth direction at these regions [284]. In this context, single-track deposition can be an effective way for melt pool morphology optimization before DED-repairing [285].

- Closing remarks

Significant advances in DED technique have been achieved in the past decades with continuous efforts made in both laboratories and industries. Compared to LB-PBF, DED process is characterized by some unique advantages which make it a more promising method for industry applications. Due to the non-equilibrium solidification process and thermal cycles, DED components consist directional columnar grains, cellular structures, elemental segregation, and high-density dislocations. In addition, some metastable phases, such as ferrite in austenite steel grades, austenite in martensitic steel grades and α’ phase in Ti alloys, are present within AB DED components. As for mechanical performance, DED components exhibit comparable or superior strength but generally inferior ductility relative to CM counterparts. In addition, the appearance of porosity and considerable surface roughness results in inferior fatigue performance (especially in HCF regime). Following additional efforts regarding to DED technique are highly desired to extend DED applications.

Significant advances were achieved in the field of LB-PBF with control on grain morphology and texture evolution, while related studies are still scarce when it comes to DED technique. In DED process, close control on microstructure evolution is challenging due to the relatively large melt pool with graded thermal field, preventing accurate local control on very small region. In this context, continuous research work is required to provide abundant experimental database on thermal field in melt pool and microstructure evolution in various DED materials. In addition, in situ HT after solidification can be interesting and promising method to adjust microstructures.

Simulation study has always been a powerful tool in scientific investigations and is also employed to help describe crystal grain evolution with various processing parameters in DED process. However, due to the rather complex thermal cycle and limitations of accessible computers, most available studies focused on single melt pool or single track, instead of multi-track layer or even multi-layer deposit. The real thermal dynamics within melt pool of blocks may deviate significantly from that of single isolated melt pool, forming gaps between simulation works and practical deposition. More accurate simulation studies with special concentration on influences of continuous thermal cycles will also help processing parameter optimization and mechanical property improvement.

As mentioned in Section 4.2, tensile properties of common DED components have been well studied, but investigations on fatigue behaviors are far from complete. Coarser structures, larger porosity with higher volume fraction and considerable surface roughness will result in disparate behaviors in DED and LB-PBF components subjected to cyclic loading. Thus, investigations on fatigue performance of DED components are necessary before extending their industrial applications.

Another challenge is that there is still no well-established standard for mechanical tests of DED blocks. Thermal histories, and therefore microstructures and mechanical performance, are known to vary significantly with processing parameters, locations where test specimens extracted as well as size and geometry of components. It is not surprising to find that there exists considerable difference among experimental data reported in available studies. Therefore, it is imperative to develop a standard for test of DED blocks with detailed description on specimen size, shape, orientation, location, and block geometry.

FGMs manufactured via DED are now compositionally gradient, instead of functionally (property) gradient. In this context, a closer control on microstructure evolution based on phase diagram and thermal field studies, rather than simply tuning composition, can be the key point in manufacturing FGMs using DED for applications.

Declaration of Competing Interest

The authors declare no conflict of interest.

Acknowledgements

XXX

References

1.	DebRoy, T., et al., Additive manufacturing of metallic components – Process, structure and properties. Progress in Materials Science, 2018. 92: p. 112-224.

2.	Frazier, W.E., Metal Additive Manufacturing: A Review. Journal of Materials Engineering and Performance, 2014. 23(6): p. 1917-1928.

3.	Gorsse, S., et al., Additive manufacturing of metals: a brief review of the characteristic microstructures and properties of steels, Ti-6Al-4V and high-entropy alloys. Sci Technol Adv Mater, 2017. 18(1): p. 584-610.

4.	Herzog, D., et al., Additive manufacturing of metals. Acta Materialia, 2016. 117: p. 371-392.

5.	Li, S., et al., 3D printing of ductile equiatomic Fe-Co alloy for soft magnetic applications. Additive Manufacturing, 2021.

6.	Kumar, P., O. Prakash, and U. Ramamurty, Micro-and meso-structures and their influence on mechanical properties of selectively laser melted Ti-6Al-4V. Acta Materialia, 2018. 154: p. 246-260.

7.	Kurzynowski, T., et al., Correlation between process parameters, microstructure and properties of 316 L stainless steel processed by selective laser melting. Materials Science and Engineering: A, 2018. 718: p. 64-73.

8.	Saboori, A., et al., How the nozzle position affects the geometry of the melt pool in directed energy deposition process. Powder Metallurgy, 2019. 62(4): p. 213-217.

9.	Martina, F., et al., Tandem metal inert gas process for high productivity wire arc additive manufacturing in stainless steel. Additive Manufacturing, 2019. 25: p. 545-550.

10.	Williams, S.W., et al., Wire + Arc Additive Manufacturing. Materials Science and Technology, 2016. 32(7): p. 641-647.

11.	Lockett, H., et al., Design for Wire + Arc Additive Manufacture: design rules and build orientation selection. Journal of Engineering Design, 2017. 28(7-9): p. 568-598.

12.	Articek, U., M. Milfelner, and I. Anzel, Synthesis of functionally graded material H13/Cu by LENS technology. Advances in Production Engineering & Management, 2013. 8(3): p. 169-176.

13.	Liu, Q., et al., Laser cladding as a potential repair technology for damaged aircraft components. International Journal of Structural Integrity, 2011. 2(3): p. 314-331.

14.	Pinkerton, A.J., W. Wang, and L. Li, Component repair using laser direct metal deposition. Proceedings of the Institution of Mechanical Engineers, Part B: Journal of Engineering Manufacture, 2008. 222(7): p. 827-836.

15.	Benarji, K., et al., Parametric investigation and characterization on SS316 built by laser-assisted directed energy deposition. Proceedings of the Institution of Mechanical Engineers, Part L: Journal of Materials: Design and Applications, 2019. 234(3): p. 452-466.

16.	Tan, H., et al., Microstructure and properties of Ti-6Al-4V fabricated by low-power pulsed laser directed energy deposition. Journal of Materials Science & Technology, 2019. 35(9): p. 2027-2037.

17.	Liu, F., et al., The effect of laser scanning path on microstructures and mechanical properties of laser solid formed nickel-base superalloy Inconel 718. Journal of Alloys and Compounds, 2011. 509(13): p. 4505-4509.

18.	Svetlizky, D., et al., Directed energy deposition (DED) additive manufacturing: Physical characteristics, defects, challenges and applications. 2021.

19.	Li, J., et al., Microstructure and performance optimisation of stainless steel formed by laser additive manufacturing. Materials Science and Technology, 2016. 32(12): p. 1223-1230.

20.	Amine, T., J.W. Newkirk, and F. Liou, An investigation of the effect of laser deposition parameters on characteristics of multilayered 316 L deposits. The International Journal of Advanced Manufacturing Technology, 2014. 73(9-12): p. 1739-1749.

21.	Tan, Z.E.E., et al., Characterisation of porosity, density, and microstructure of directed energy deposited stainless steel AISI 316L. Additive Manufacturing, 2019. 25: p. 286-296.

22.	Xue, Y., et al., Microporosity effects on cyclic plasticity and fatigue of LENS™-processed steel. Acta Materialia, 2010. 58(11): p. 4029-4038.

23.	Yadollahi, A., et al., Effects of process time interval and heat treatment on the mechanical and microstructural properties of direct laser deposited 316L stainless steel. Materials Science and Engineering: A, 2015. 644: p. 171-183.

24.	Zhang, Q., et al., Grain morphology control and texture characterization of laser solid formed Ti6Al2Sn2Zr3Mo1.5Cr2Nb titanium alloy. Journal of Materials Processing Technology, 2016. 238: p. 202-211.

25.	Qiu, C., G.A. Ravi, and M.M. Attallah, Microstructural control during direct laser deposition of a β-titanium alloy. Materials & Design, 2015. 81: p. 21-30.

26.	Wang, T., et al., Grain morphology evolution behavior of titanium alloy components during laser melting deposition additive manufacturing. Journal of Alloys and Compounds, 2015. 632: p. 505-513.

27.	Wu, X., et al., Microstructure and properties of a laser fabricated burn-resistant Ti alloy. Materials & Design, 2004. 25(2): p. 103-109.

28.	Saboori, A., et al., An investigation on the effect of deposition pattern on the microstructure, mechanical properties and residual stress of 316L produced by Directed Energy Deposition. Materials Science and Engineering: A, 2020. 780.

29.	Saboori, A., et al., An investigation on the effect of powder recycling on the microstructure and mechanical properties of AISI 316L produced by Directed Energy Deposition. Materials Science and Engineering: A, 2019. 766.

30.	Zhang, K., W. Liu, and X. Shang, Research on the processing experiments of laser metal deposition shaping. Optics & Laser Technology, 2007. 39(3): p. 549-557.

31.	Zhang, J., et al., Fatigue crack propagation behaviour in wire+arc additive manufactured Ti‐6Al‐4V: Effects of microstructure and residual stress. Materials & Design, 2016. 90: p. 551-561.

32.	Syed, W.U.H., A.J. Pinkerton, and L. Li, Combining wire and coaxial powder feeding in laser direct metal deposition for rapid prototyping. Applied Surface Science, 2006. 252(13): p. 4803-4808.

33.	Bhattacharya, S., et al., Microstructural evolution and mechanical, and corrosion property evaluation of Cu–30Ni alloy formed by Direct Metal Deposition process. Journal of Alloys and Compounds, 2011. 509(22): p. 6364-6373.

34.	Imran, M.K., et al., Direct metal deposition (DMD) of H13 tool steel on copper alloy substrate: Evaluation of mechanical properties. Materials Science and Engineering: A, 2011. 528(9): p. 3342-3349.

35.	Liu, F., et al., Microstructural changes in a laser solid forming Inconel 718 superalloy thin wall in the deposition direction. Optics & Laser Technology, 2013. 45: p. 330-335.

36.	Horgar, A., et al., Additive manufacturing using WAAM with AA5183 wire. Journal of Materials Processing Technology, 2018. 259: p. 68-74.

37.	Xiong, J., et al., Influences of process parameters on surface roughness of multi-layer single-pass thin-walled parts in GMAW-based additive manufacturing. Journal of Materials Processing Technology, 2018. 252: p. 128-136.

38.	Brandl, E., et al., Mechanical properties of additive manufactured titanium (Ti–6Al–4V) blocks deposited by a solid-state laser and wire. Materials & Design, 2011. 32(10): p. 4665-4675.

39.	Brandl, E., A. Schoberth, and C. Leyens, Morphology, microstructure, and hardness of titanium (Ti-6Al-4V) blocks deposited by wire-feed additive layer manufacturing (ALM). Materials Science and Engineering: A, 2012. 532: p. 295-307.

40.	Butler, T.M., et al., Evolution of Texture from a Single Crystal Ti-6Al-4V Substrate During Electron Beam Directed Energy Deposition. Metallurgical and Materials Transactions A, 2017. 48(10): p. 4441-4446.

41.	Zhang, J., et al., Crack path selection at the interface of wrought and wire+arc additive manufactured Ti–6Al–4V. Materials & Design, 2016. 104: p. 365-375.

42.	Moore, P., A. Addison, and M. Nowak-Coventry, Mechanical properties of wire plus arc additive manufactured steel and stainless steel structures. Welding in the World, 2019. 63(6): p. 1521-1530.

43.	Ma, M., Z. Wang, and X. Zeng, A comparison on metallurgical behaviors of 316L stainless steel by selective laser melting and laser cladding deposition. Materials Science and Engineering: A, 2017. 685: p. 265-273.

44.	Zheng, B., et al., On the evolution of microstructure and defect control in 316L SS components fabricated via directed energy deposition. Materials Science and Engineering: A, 2019. 764.

45.	Sampson, R., et al., The influence of key process parameters on melt pool geometry in direct energy deposition additive manufacturing systems. Optics & Laser Technology, 2021. 134.

46.	Yuan, K., et al., Influence of process parameters and heat treatments on the microstructures and dynamic mechanical behaviors of Inconel 718 superalloy manufactured by laser metal deposition. Materials Science and Engineering: A, 2018. 721: p. 215-225.

47.	Baufeld, B., E. Brandl, and O. van der Biest, Wire based additive layer manufacturing: Comparison of microstructure and mechanical properties of Ti–6Al–4V components fabricated by laser-beam deposition and shaped metal deposition. Journal of Materials Processing Technology, 2011. 211(6): p. 1146-1158.

48.	Yao, M., et al., Effect of deposition modes on electron beam directed energy deposited inconel 718. Materials Science and Technology, 2020. 36(14): p. 1556-1565.

49.	Stawovy, M.T., Comparison of LCAC and PM Mo deposited using Sciaky EBAM™. International Journal of Refractory Metals and Hard Materials, 2018. 73: p. 162-167.

50.	Laghi, V., et al., On the influence of the geometrical irregularities in the mechanical response of Wire-and-Arc Additively Manufactured planar elements. Journal of Constructional Steel Research, 2021. 178.

51.	Martina, F., et al., Residual stress of as-deposited and rolled wire+arc additive manufacturing Ti–6Al–4V components. Materials Science and Technology, 2016. 32(14): p. 1439-1448.

52.	Amato, K.N., et al., Microstructures and mechanical behavior of Inconel 718 fabricated by selective laser melting. Acta Materialia, 2012. 60(5): p. 2229-2239.

53.	Deng, D., et al., Microstructure and mechanical properties of Inconel 718 produced by selective laser melting: Sample orientation dependence and effects of post heat treatments. Materials Science and Engineering: A, 2018. 713: p. 294-306.

54.	Liverani, E., et al., Effect of selective laser melting (SLM) process parameters on microstructure and mechanical properties of 316L austenitic stainless steel. Journal of Materials Processing Technology, 2017. 249: p. 255-263.

55.	Sun, Z., et al., Selective laser melting of stainless steel 316L with low porosity and high build rates. Materials & Design, 2016. 104: p. 197-204.

56.	Cheng, B. and K. Chou. Melt pool evolution study in selective laser melting. in 26th Annual International Solid Freeform Fabrication Symposium-An Additive Manufacturing Conference, Austin, TX, USA. 2015.

57.	Heeling, T., M. Cloots, and K. Wegener, Melt pool simulation for the evaluation of process parameters in selective laser melting. Additive Manufacturing, 2017. 14: p. 116-125.

58.	Charles, A., et al., Effect of Process Parameters on the Generated Surface Roughness of Down-Facing Surfaces in Selective Laser Melting. Applied Sciences, 2019. 9(6).

59.	Yu, W., et al., Influence of re-melting on surface roughness and porosity of AlSi10Mg parts fabricated by selective laser melting. Journal of Alloys and Compounds, 2019. 792: p. 574-581.

60.	Yilmaz, O. and A.A. Ugla, Shaped metal deposition technique in additive manufacturing: A review. Proceedings of the Institution of Mechanical Engineers, Part B: Journal of Engineering Manufacture, 2016. 230(10): p. 1781-1798.

61.	Dass, A. and A. Moridi, State of the Art in Directed Energy Deposition: From Additive Manufacturing to Materials Design. Coatings, 2019. 9(7).

62.	Wang, Z.D., et al., Investigation of the underwater laser directed energy deposition technique for the on-site repair of HSLA-100 steel with excellent performance. Additive Manufacturing, 2021. 39.

63.	Sames, W.J., et al., The metallurgy and processing science of metal additive manufacturing. International Materials Reviews, 2016. 61(5): p. 315-360.

64.	Kelly, J.P., et al., Directed energy deposition additive manufacturing of functionally graded Al-W composites. Additive Manufacturing, 2021. 39.

65.	Dev Singh, D., S. Arjula, and A. Raji Reddy, Functionally Graded Materials Manufactured by Direct Energy Deposition: A review. Materials Today: Proceedings, 2021.

66.	Guo, C., et al., A comparing study of defect generation in IN738LC superalloy fabricated by laser powder bed fusion: Continuous-wave mode versus pulsed-wave mode. Journal of Materials Science & Technology, 2021. 90: p. 45-57.

67.	Akbari, M. and R. Kovacevic, Closed loop control of melt pool width in robotized laser powder–directed energy deposition process. The International Journal of Advanced Manufacturing Technology, 2019. 104(5-8): p. 2887-2898.

68.	Khanzadeh, M., et al., In-situ monitoring of melt pool images for porosity prediction in directed energy deposition processes. IISE Transactions, 2018. 51(5): p. 437-455.

69.	Qi, H., J. Mazumder, and H. Ki, Numerical simulation of heat transfer and fluid flow in coaxial laser cladding process for direct metal deposition. Journal of Applied Physics, 2006. 100(2).

70.	Shim, D.-S., et al., Effect of layer thickness setting on deposition characteristics in direct energy deposition (DED) process. Optics & Laser Technology, 2016. 86: p. 69-78.

71.	Kurnsteiner, P., et al., High-strength Damascus steel by additive manufacturing. Nature, 2020. 582(7813): p. 515-519.

72.	Todaro, C.J., et al., Grain structure control during metal 3D printing by high-intensity ultrasound. Nature Communications, 2020. 11(1).

73.	Todaro, C.J., et al., Grain refinement of stainless steel in ultrasound-assisted additive manufacturing. Additive Manufacturing, 2021. 37.

74.	Nursyifaulkhair, D., et al., Influence of cooling rate on volume fraction of α massive phase in a Ti-6Al-4V alloy fabricated using directed energy deposition. Materials Letters, 2019. 257.

75.	Mukherjee, T., et al., Printability of alloys for additive manufacturing. Sci Rep, 2016. 6: p. 19717.

76.	Sun, G., et al., Evaluation of defect density, microstructure, residual stress, elastic modulus, hardness and strength of laser-deposited AISI 4340 steel. Acta Materialia, 2015. 84: p. 172-189.

77.	Akbari, M. and R. Kovacevic, An investigation on mechanical and microstructural properties of 316LSi parts fabricated by a robotized laser/wire direct metal deposition system. Additive Manufacturing, 2018. 23: p. 487-497.

78.	Chen, G., et al., A comparative study of Ti-6Al-4V powders for additive manufacturing by gas atomization, plasma rotating electrode process and plasma atomization. Powder Technology, 2018. 333: p. 38-46.

79.	Pang, S., W. Chen, and W. Wang, A Quantitative Model of Keyhole Instability Induced Porosity in Laser Welding of Titanium Alloy. Metallurgical and Materials Transactions A, 2014. 45(6): p. 2808-2818.

80.	Ng, G., et al., Porosity formation and gas bubble retention in laser metal deposition. 2009. 97(3): p. 641-649.

81.	Susan, D., et al., Quantitative characterization of porosity in stainless steel LENS powders and deposits. 2006. 57(1): p. 36-43.

82.	Fujishima, M., et al., Study on factors for pores and cladding shape in the deposition processes of Inconel 625 by the directed energy deposition (DED) method. 2017. 19: p. 200-204.

83.	Panwisawas, C., et al., Keyhole formation and thermal fluid flow-induced porosity during laser fusion welding in titanium alloys: Experimental and modelling. 2017. 126: p. 251-263.

84.	Ahsan, M.N., R. Bradley, and A.J.J.J.o.l.a. Pinkerton, Microcomputed tomography analysis of intralayer porosity generation in laser direct metal deposition and its causes. 2011. 23(2): p. 022009.

85.	Ronneberg, T., C.M. Davies, and P.A. Hooper, Revealing relationships between porosity, microstructure and mechanical properties of laser powder bed fusion 316L stainless steel through heat treatment. Materials & Design, 2020. 189.

86.	Darvish, K., Z.W. Chen, and T. Pasang, Reducing lack of fusion during selective laser melting of CoCrMo alloy: Effect of laser power on geometrical features of tracks. Materials & Design, 2016. 112: p. 357-366.

87.	Buza, G., et al., On the Possible Mechanisms of Porosity Formation during Laser Melt Injection (LMI) Technology. Materials Science Forum, 2008. 589: p. 79-84.

88.	Aghion, E. and B. Bronfin, Magnesium Alloys Development towards the 21<sup>st</sup> Century. Materials Science Forum, 2000. 350-351: p. 19-30.

89.	Lin, R., et al., Numerical study of keyhole dynamics and keyhole-induced porosity formation in remote laser welding of Al alloys. 2017. 108: p. 244-256.

90.	Bai, L., et al., Grain morphologies and microstructures of laser melting deposited V-5Cr-5Ti alloys. Journal of Alloys and Compounds, 2018. 745: p. 716-724.

91.	Ma, M., Z. Wang, and X. Zeng, Effect of energy input on microstructural evolution of direct laser fabricated IN718 alloy. Materials Characterization, 2015. 106: p. 420-427.

92.	Qi, H., M. Azer, and A. Ritter, Studies of Standard Heat Treatment Effects on Microstructure and Mechanical Properties of Laser Net Shape Manufactured INCONEL 718. Metallurgical and Materials Transactions A, 2009. 40(10): p. 2410-2422.

93.	Wolff, S.J., et al., A framework to link localized cooling and properties of directed energy deposition (DED)-processed Ti-6Al-4V. Acta Materialia, 2017. 132: p. 106-117.

94.	Thomas, M., G.J. Baxter, and I. Todd, Normalised model-based processing diagrams for additive layer manufacture of engineering alloys. Acta Materialia, 2016. 108: p. 26-35.

95.	Leung, C.L.A., et al., In situ X-ray imaging of defect and molten pool dynamics in laser additive manufacturing. Nat Commun, 2018. 9(1): p. 1355.

96.	Mazumder, J.J.O.e., Overview of melt dynamics in laser processing. 1991. 30(8): p. 1208-1219.

97.	Antony, K. and N.J.J.E.S.T. Arivazhagan, Studies on energy penetration and Marangoni effect during laser melting process. 2015. 10(4): p. 509-525.

98.	Ansari, M., et al., Laser directed energy deposition of water-atomized iron powder: Process optimization and microstructure of single-tracks. Optics & Laser Technology, 2019. 112: p. 485-493.

99.	Zhong, C., et al., Experimental study of porosity reduction in high deposition-rate Laser Material Deposition. Optics & Laser Technology, 2015. 75: p. 87-92.

100.	Aggarwal, A., et al., Role of impinging powder particles on melt pool hydrodynamics, thermal behaviour and microstructure in laser-assisted DED process: A particle-scale DEM – CFD – CA approach. International Journal of Heat and Mass Transfer, 2020. 158.

101.	Svetlizky, D., et al., Directed energy deposition of Al 5xxx alloy using Laser Engineered Net Shaping (LENS®). Materials & Design, 2020. 192.

102.	Sufiiarov, V.S., et al., The Effect of Layer Thickness at Selective Laser Melting. Procedia Engineering, 2017. 174: p. 126-134.

103.	Kou, S.J.N.J., USA, Welding metallurgy. 2003: p. 431-446.

104.	Gäumann, M., et al., Single-crystal laser deposition of superalloys: processing–microstructure maps. 2001. 49(6): p. 1051-1062.

105.	Gäumann, M., et al., Epitaxial laser metal forming: analysis of microstructure formation. 1999. 271(1-2): p. 232-241.

106.	Du, D., et al., Influence of build orientation on microstructure, mechanical and corrosion behavior of Inconel 718 processed by selective laser melting. Materials Science and Engineering: A, 2019. 760: p. 469-480.

107.	Helmer, H., et al., Grain structure evolution in Inconel 718 during selective electron beam melting. Materials Science and Engineering: A, 2016. 668: p. 180-187.

108.	Wei, H.L., J. Mazumder, and T. DebRoy, Evolution of solidification texture during additive manufacturing. Sci Rep, 2015. 5: p. 16446.

109.	Dinda, G.P., A.K. Dasgupta, and J. Mazumder, Texture control during laser deposition of nickel-based superalloy. Scripta Materialia, 2012. 67(5): p. 503-506.

110.	Criales, L.E., et al., Laser powder bed fusion of nickel alloy 625: Experimental investigations of effects of process parameters on melt pool size and shape with spatter analysis. International Journal of Machine Tools and Manufacture, 2017. 121: p. 22-36.

111.	Guo, Q., et al., In-situ characterization and quantification of melt pool variation under constant input energy density in laser powder bed fusion additive manufacturing process. Additive Manufacturing, 2019. 28: p. 600-609.

112.	Song, L., et al., Control of melt pool temperature and deposition height during direct metal deposition process. The International Journal of Advanced Manufacturing Technology, 2011. 58(1-4): p. 247-256.

113.	Dinda, G.P., A.K. Dasgupta, and J. Mazumder, Evolution of microstructure in laser deposited Al–11.28%Si alloy. Surface and Coatings Technology, 2012. 206(8-9): p. 2152-2160.

114.	Carroll, B.E., T.A. Palmer, and A.M. Beese, Anisotropic tensile behavior of Ti–6Al–4V components fabricated with directed energy deposition additive manufacturing. Acta Materialia, 2015. 87: p. 309-320.

115.	Kok, Y., et al., Anisotropy and heterogeneity of microstructure and mechanical properties in metal additive manufacturing: A critical review. Materials & Design, 2018. 139: p. 565-586.

116.	Schempp, P., et al., Solidification of GTA aluminum weld metal: Part 1—Grain morphology dependent upon alloy composition and grain refiner content. 2014. 93(2): p. 53s-59s.

117.	Wei, H.L., J.W. Elmer, and T. DebRoy, Origin of grain orientation during solidification of an aluminum alloy. Acta Materialia, 2016. 115: p. 123-131.

118.	Wang, Y., J. Shi, and Y. Liu, Competitive grain growth and dendrite morphology evolution in selective laser melting of Inconel 718 superalloy. Journal of Crystal Growth, 2019. 521: p. 15-29.

119.	Zhang, Q., et al., Solidification Microstructure of Laser Additive Manufactured Ti6Al2Zr2Sn3Mo1.5Cr2Nb Titanium Alloy. Journal of Materials Science & Technology, 2016. 32(4): p. 381-386.

120.	Banerjee, R., et al., Direct laser deposition of in situ Ti–6Al–4V–TiB composites. Materials Science and Engineering: A, 2003. 358(1-2): p. 343-349.

121.	Novichenko, D., et al., Metal Matrix Composite Material by Direct Metal Deposition. Physics Procedia, 2011. 12: p. 296-302.

122.	Pouzet, S., et al., Additive layer manufacturing of titanium matrix composites using the direct metal deposition laser process. Materials Science and Engineering: A, 2016. 677: p. 171-181.

123.	Xue, A., et al., Influence of trace boron addition on microstructure, tensile properties and their anisotropy of Ti6Al4V fabricated by laser directed energy deposition. Materials & Design, 2019. 181.

124.	Zhang, Y., J. Sun, and R. Vilar, Characterization of (TiB+TiC)/TC4 in situ titanium matrix composites prepared by laser direct deposition. Journal of Materials Processing Technology, 2011. 211(4): p. 597-601.

125.	Mereddy, S., et al., Grain refinement of wire arc additively manufactured titanium by the addition of silicon. Journal of Alloys and Compounds, 2017. 695: p. 2097-2103.

126.	Bermingham, M.J., et al., Promoting the columnar to equiaxed transition and grain refinement of titanium alloys during additive manufacturing. Acta Materialia, 2019. 168: p. 261-274.

127.	Wang, Y., et al., Microstructure and mechanical properties of TiN particles strengthened 316L steel prepared by laser melting deposition process. Materials Science and Engineering: A, 2021. 814.

128.	Wilson, J.M. and Y.C. Shin, Microstructure and wear properties of laser-deposited functionally graded Inconel 690 reinforced with TiC. Surface and Coatings Technology, 2012. 207: p. 517-522.

129.	Xu, J., et al., Assembly of metals and nanoparticles into novel nanocomposite superstructures. Scientific Reports, 2013. 3(1).

130.	Karantzalis, A.E., et al., Casting-Based Production of Al-TiC-AlB2 Composite Material Through the Use of KBF4 Salt. Journal of Materials Engineering and Performance, 2010. 20(2): p. 198-202.

131.	Liu, Q., et al., Corrosion behaviour of 316H stainless steel in molten FLiNaK eutectic salt containing graphite particles. Corrosion Science, 2019. 160.

132.	Kuang, W. and G.S. Was, The effects of grain boundary carbide density and strain rate on the stress corrosion cracking behavior of cold rolled Alloy 690. Corrosion Science, 2015. 97: p. 107-114.

133.	Liu, Z. and H. Qi, Effects of substrate crystallographic orientations on crystal growth and microstructure formation in laser powder deposition of nickel-based superalloy. Acta Materialia, 2015. 87: p. 248-258.

134.	Vilar, R. and A. Almeida, Repair and manufacturing of single crystal Ni-based superalloys components by laser powder deposition—A review. Journal of Laser Applications, 2015. 27(S1).

135.	Ziętala, M., et al., The microstructure, mechanical properties and corrosion resistance of 316L stainless steel fabricated using laser engineered net shaping. Materials Science and Engineering: A, 2016. 677: p. 1-10.

136.	Smith, T.R., et al., Strengthening mechanisms in directed energy deposited austenitic stainless steel. Acta Materialia, 2019. 164: p. 728-740.

137.	Li, Y., et al., Multi-scale microstructural investigation of a laser 3D printed Ni-based superalloy. Additive Manufacturing, 2020. 34.

138.	Fu, J.W., et al., Effect of cooling rate on solidification microstructures in AISI 304 stainless steel. Materials Science and Technology, 2013. 24(8): p. 941-944.

139.	Ganesh, P., et al., Studies on pitting corrosion and sensitization in laser rapid manufactured specimens of type 316L stainless steel. Materials & Design, 2012. 39: p. 509-521.

140.	Aveson, J.W., et al., On the origin of sliver defects in single crystal investment castings. Acta Materialia, 2013. 61(14): p. 5162-5171.

141.	Wang, G., et al., Variation of crystal orientation during epitaxial growth of dendrites by laser deposition. Journal of Materials Science & Technology, 2018. 34(4): p. 732-735.

142.	Suprobo, G., et al., Thermal Decomposition of Massive Phase to Fine Lamellar α/β in Ti–6Al–4V Additively Manufactured Alloy by Directed Energy Deposition. Metals and Materials International, 2019. 25(6): p. 1428-1435.

143.	Kustas, A.B., et al., Characterization of the Fe-Co-1.5V soft ferromagnetic alloy processed by Laser Engineered Net Shaping (LENS). Additive Manufacturing, 2018. 21: p. 41-52.

144.	Babuska, T.F., et al., Comparison of powder bed fusion and directed energy deposition for tailoring mechanical properties of traditionally brittle alloys. Manufacturing Letters, 2021. 28: p. 30-34.

145.	Wang, Y.M., et al., Additively manufactured hierarchical stainless steels with high strength and ductility. Nat Mater, 2018. 17(1): p. 63-71.

146.	Kim, H.S., et al., Effect of cooling rate on microstructure evolution of rapidly cooled high-impurity steels. Materials Science and Engineering: A, 2005. 403(1-2): p. 311-317.

147.	Yin, H. and S.D. Felicelli, Dendrite growth simulation during solidification in the LENS process. Acta Materialia, 2010. 58(4): p. 1455-1465.

148.	Rafi, H.K., et al., Microstructures and Mechanical Properties of Ti6Al4V Parts Fabricated by Selective Laser Melting and Electron Beam Melting. Journal of Materials Engineering and Performance, 2013. 22(12): p. 3872-3883.

149.	Bertsch, K.M., et al., Origin of dislocation structures in an additively manufactured austenitic stainless steel 316L. Acta Materialia, 2020. 199: p. 19-33.

150.	Kumara, C., et al., Microstructure modelling of laser metal powder directed energy deposition of alloy 718. Additive Manufacturing, 2019. 25: p. 357-364.

151.	Barkia, B., et al., On the origin of the high tensile strength and ductility of additively manufactured 316L stainless steel: Multiscale investigation. Journal of Materials Science & Technology, 2020. 41: p. 209-218.

152.	Pham, M.S., et al., Dislocation structure evolution and its effects on cyclic deformation response of AISI 316L stainless steel. Materials Science and Engineering: A, 2011. 528(7-8): p. 3261-3269.

153.	Kong, D., et al., About metastable cellular structure in additively manufactured austenitic stainless steels. Additive Manufacturing, 2021. 38.

154.	Li, S.-H., et al., Small-volume aluminum alloys with native oxide shell deliver unprecedented strength and toughness. Acta Materialia, 2017. 126: p. 202-209.

155.	Pokharel, R., et al., Signatures of the unique microstructure of additively manufactured steel observed via diffraction. Scripta Materialia, 2018. 155: p. 16-20.

156.	Bronkhorst, C.A., et al., Structural representation of additively manufactured 316L austenitic stainless steel. International Journal of Plasticity, 2019. 118: p. 70-86.

157.	Brown, D.W., et al., Using In Situ Neutron Diffraction to Isolate Specific Features of Additively Manufactured Microstructures in 304L Stainless Steel and Identify Their Effects on Macroscopic Strength. Metallurgical and Materials Transactions A, 2019. 50(7): p. 3399-3413.

158.	Hu, Y., et al., Microstructural evolution and anisotropic mechanical properties of Inconel 625 superalloy fabricated by directed energy deposition. Journal of Alloys and Compounds, 2021. 870.

159.	Yin, Y.J., et al., Mechanism of high yield strength and yield ratio of 316 L stainless steel by additive manufacturing. Materials Science and Engineering: A, 2019. 744: p. 773-777.

160.	Godec, M., et al., Quantitative multiscale correlative microstructure analysis of additive manufacturing of stainless steel 316L processed by selective laser melting. Materials Characterization, 2020. 160.

161.	Cui, L., et al., Revealing relationships between microstructure and hardening nature of additively manufactured 316L stainless steel. Materials & Design, 2021. 198.

162.	Ghayoor, M., et al., Selective laser melting of austenitic oxide dispersion strengthened steel: Processing, microstructural evolution and strengthening mechanisms. Materials Science and Engineering: A, 2020. 788.

163.	Peyrouzet, F., et al., Selective Laser Melting of Al0.3CoCrFeNi High-Entropy Alloy: Printability, Microstructure, and Mechanical Properties. Jom, 2019. 71(10): p. 3443-3451.

164.	Bajaj, P., et al., Steels in additive manufacturing: A review of their microstructure and properties. Materials Science and Engineering: A, 2020. 772.

165.	Zhong, Y., et al., Intragranular cellular segregation network structure strengthening 316L stainless steel prepared by selective laser melting. Journal of Nuclear Materials, 2016. 470: p. 170-178.

166.	Murr, L.E., et al., Microstructures and Properties of 17-4 PH Stainless Steel Fabricated by Selective Laser Melting. Journal of Materials Research and Technology, 2012. 1(3): p. 167-177.

167.	Wang, D., et al., The effects of fabrication atmosphere condition on the microstructural and mechanical properties of laser direct manufactured stainless steel 17-4 PH. Journal of Materials Science & Technology, 2019. 35(7): p. 1315-1322.

168.	Yu, Z., et al., Effect of laser remelting processing on microstructure and mechanical properties of 17-4 PH stainless steel during laser direct metal deposition. Journal of Materials Processing Technology, 2020. 284.

169.	Mathoho, I., et al., Impact of DED process parameters on the metallurgical characteristics of 17-4 PH SS deposited using DED. CIRP Journal of Manufacturing Science and Technology, 2020. 31: p. 450-458.

170.	Mirzadeh, H. and A. Najafizadeh, Aging kinetics of 17-4 PH stainless steel. Materials Chemistry and Physics, 2009. 116(1): p. 119-124.

171.	LeBrun, T., et al., Effect of retained austenite on subsequent thermal processing and resultant mechanical properties of selective laser melted 17–4 PH stainless steel. Materials & Design, 2015. 81: p. 44-53.

172.	Facchini, L., et al., Metastable Austenite in 17-4 Precipitation-Hardening Stainless Steel Produced by Selective Laser Melting. Advanced Engineering Materials, 2010. 12(3): p. 184-188.

173.	Yadollahi, A., et al., Effects of building orientation and heat treatment on fatigue behavior of selective laser melted 17-4 PH stainless steel. International Journal of Fatigue, 2017. 94: p. 218-235.

174.	Meredith, S.D., et al., Impact of composition on the heat treatment response of additively manufactured 17–4 PH grade stainless steel. Materials Science and Engineering: A, 2018. 738: p. 44-56.

175.	Kumar, P. and U. Ramamurty, Microstructural optimization through heat treatment for enhancing the fracture toughness and fatigue crack growth resistance of selective laser melted Ti 6Al 4V alloy. Acta Materialia, 2019. 169: p. 45-59.

176.	Tan, X., et al., Graded microstructure and mechanical properties of additive manufactured Ti–6Al–4V via electron beam melting. Acta Materialia, 2015. 97: p. 1-16.

177.	Yao, B., et al., Microstructure and mechanical properties of Ti-6Al-4V components fabricated by laser micro cladding deposition. Rare Metals, 2015. 34(7): p. 445-451.

178.	Qiu, C., et al., Fabrication of large Ti–6Al–4V structures by direct laser deposition. Journal of Alloys and Compounds, 2015. 629: p. 351-361.

179.	Keist, J.S. and T.A. Palmer, Role of geometry on properties of additively manufactured Ti-6Al-4V structures fabricated using laser based directed energy deposition. Materials & Design, 2016. 106: p. 482-494.

180.	Zhai, Y., H. Galarraga, and D.A. Lados, Microstructure Evolution, Tensile Properties, and Fatigue Damage Mechanisms in Ti-6Al-4V Alloys Fabricated by Two Additive Manufacturing Techniques. Procedia Engineering, 2015. 114: p. 658-666.

181.	Sridharan, N., et al., Texture Evolution During Laser Direct Metal Deposition of Ti-6Al-4V. Jom, 2016. 68(3): p. 772-777.

182.	Facchini, L., et al., Ductility of a Ti‐6Al‐4V alloy produced by selective laser melting of prealloyed powders. Rapid Prototyping Journal, 2010. 16(6): p. 450-459.

183.	Vilaro, T., C. Colin, and J.D. Bartout, As-Fabricated and Heat-Treated Microstructures of the Ti-6Al-4V Alloy Processed by Selective Laser Melting. Metallurgical and Materials Transactions A, 2011. 42(10): p. 3190-3199.

184.	Xu, W., et al., Additive manufacturing of strong and ductile Ti–6Al–4V by selective laser melting via in situ martensite decomposition. Acta Materialia, 2015. 85: p. 74-84.

185.	Koike, M., et al., Evaluation of Titanium Alloys Fabricated Using Rapid Prototyping Technologies-Electron Beam Melting and Laser Beam Melting. Materials (Basel), 2011. 4(10): p. 1776-1792.

186.	Brandl, E., C. Leyens, and F. Palm, Mechanical Properties of Additive Manufactured Ti-6Al-4V Using Wire and Powder Based Processes. IOP Conference Series: Materials Science and Engineering, 2011. 26.

187.	Alcisto, J., et al., Tensile Properties and Microstructures of Laser-Formed Ti-6Al-4V. Journal of Materials Engineering and Performance, 2010. 20(2): p. 203-212.

188.	Ahmed, T., H.J.M.S. Rack, and E. A, Phase transformations during cooling in α+ β titanium alloys. 1998. 243(1-2): p. 206-211.

189.	Rombouts, M., et al., Laser metal deposition of Inconel 625: Microstructure and mechanical properties. Journal of Laser Applications, 2012. 24(5).

190.	Blackwell, P.L., The mechanical and microstructural characteristics of laser-deposited IN718. Journal of Materials Processing Technology, 2005. 170(1-2): p. 240-246.

191.	Jinoop, A.N., et al., Laser Additive Manufacturing using directed energy deposition of Inconel-718 wall structures with tailored characteristics. Vacuum, 2019. 166: p. 270-278.

192.	Kakinuma, Y., et al., Influence of metal powder characteristics on product quality with directed energy deposition of Inconel 625. CIRP Annals, 2016. 65(1): p. 209-212.

193.	Tian, Y., et al., Rationalization of Microstructure Heterogeneity in INCONEL 718 Builds Made by the Direct Laser Additive Manufacturing Process. Metallurgical and Materials Transactions A, 2014. 45(10): p. 4470-4483.

194.	Sui, S., et al., The tensile deformation behavior of laser repaired Inconel 718 with a non-uniform microstructure. Materials Science and Engineering: A, 2017. 688: p. 480-487.

195.	Johnson, A.S., et al., Microstructure, Fatigue Behavior, and Failure Mechanisms of Direct Laser-Deposited Inconel 718. Jom, 2016. 69(3): p. 597-603.

196.	Yu, X., et al., Influence of post-heat-treatment on the microstructure and fracture toughness properties of Inconel 718 fabricated with laser directed energy deposition additive manufacturing. Materials Science and Engineering: A, 2020. 798.

197.	Zhong, C., et al., Improvement of material performance of Inconel 718 formed by high deposition-rate laser metal deposition. Materials & Design, 2016. 98: p. 128-134.

198.	Zhao, X., et al., Study on microstructure and mechanical properties of laser rapid forming Inconel 718. Materials Science and Engineering: A, 2008. 478(1-2): p. 119-124.

199.	Huang, W., et al., Heat treatment of Inconel 718 produced by selective laser melting: Microstructure and mechanical properties. Materials Science and Engineering: A, 2019. 750: p. 98-107.

200.	Xiao, H., et al., Effects of laser modes on Nb segregation and Laves phase formation during laser additive manufacturing of nickel-based superalloy. Materials Letters, 2017. 188: p. 260-262.

201.	Nie, P., O.A. Ojo, and Z. Li, Numerical modeling of microstructure evolution during laser additive manufacturing of a nickel-based superalloy. Acta Materialia, 2014. 77: p. 85-95.

202.	Ma, K., et al., Mechanical behavior and strengthening mechanisms in ultrafine grain precipitation-strengthened aluminum alloy. Acta Materialia, 2014. 62: p. 141-155.

203.	Yasi, J.A., L.G. Hector, and D.R. Trinkle, First-principles data for solid-solution strengthening of magnesium: From geometry and chemistry to properties. Acta Materialia, 2010. 58(17): p. 5704-5713.

204.	Smith, T.R., et al., Anomalous Annealing Response of Directed Energy Deposited Type 304L Austenitic Stainless Steel. Jom, 2018. 70(3): p. 358-363.

205.	Cahn, J.W. Hardening by spinodal decomposition. in Symposium on the Role of Substructure in the Mechanical Behavior of Metals. 1963.

206.	Wang, X., et al., Microstructure and mechanical properties of stainless steel 316L vertical struts manufactured by laser powder bed fusion process. Materials Science and Engineering: A, 2018. 736: p. 27-40.

207.	Zhu, Z.G., et al., Selective laser melting enabling the hierarchically heterogeneous microstructure and excellent mechanical properties in an interstitial solute strengthened high entropy alloy. Materials Research Letters, 2019. 7(11): p. 453-459.

208.	Li, Z., B. He, and Q. Guo, Strengthening and hardening mechanisms of additively manufactured stainless steels: The role of cell sizes. Scripta Materialia, 2020. 177: p. 17-21.

209.	Liu, L., et al., Dislocation network in additive manufactured steel breaks strength–ductility trade-off. Materials Today, 2018. 21(4): p. 354-361.

210.	Ma, M., et al., Control of shape and performance for direct laser fabrication of precision large-scale metal parts with 316L Stainless Steel. Optics & Laser Technology, 2013. 45: p. 209-216.

211.	Yu, J., M. Rombouts, and G. Maes, Cracking behavior and mechanical properties of austenitic stainless steel parts produced by laser metal deposition. Materials & Design, 2013. 45: p. 228-235.

212.	Zhang, Y., et al., Characterization of laser direct deposited metallic parts. Journal of Materials Processing Technology, 2003. 142(2): p. 582-585.

213.	Bartolomeu, F., et al., 316L stainless steel mechanical and tribological behavior—A comparison between selective laser melting, hot pressing and conventional casting. Additive Manufacturing, 2017. 16: p. 81-89.

214.	Tolosa, I., et al., Study of mechanical properties of AISI 316 stainless steel processed by “selective laser melting”, following different manufacturing strategies. 2010. 51(5): p. 639-647.

215.	Wang, Z., T.A. Palmer, and A.M. Beese, Effect of processing parameters on microstructure and tensile properties of austenitic stainless steel 304L made by directed energy deposition additive manufacturing. Acta Materialia, 2016. 110: p. 226-235.

216.	Carlton, H.D., et al., Damage evolution and failure mechanisms in additively manufactured stainless steel. Materials Science and Engineering: A, 2016. 651: p. 406-414.

217.	Suryawanshi, J., K.G. Prashanth, and U. Ramamurty, Mechanical behavior of selective laser melted 316L stainless steel. Materials Science and Engineering: A, 2017. 696: p. 113-121.

218.	Deev, A.A., P.A. Kuznetcov, and S.N. Petrov, Anisotropy of Mechanical Properties and its Correlation with the Structure of the Stainless Steel 316L Produced by the SLM Method. Physics Procedia, 2016. 83: p. 789-796.

219.	Mertens, A., et al., Mechanical properties of alloy Ti–6Al–4V and of stainless steel 316L processed by selective laser melting: influence of out-of-equilibrium microstructures. Powder Metallurgy, 2014. 57(3): p. 184-189.

220.	Caballero, A., et al., Wire + Arc Additive Manufacture of 17-4 PH stainless steel: Effect of different processing conditions on microstructure, hardness, and tensile strength. Journal of Materials Processing Technology, 2019. 268: p. 54-62.

221.	Wu, J.-H. and C.-K.J.J.o.m.s. Lin, Influence of high temperature exposure on the mechanical behavior and microstructure of 17-4 PH stainless steel. 2003. 38(5): p. 965-971.

222.	Rafi, H.K., et al., Microstructure and Mechanical Behavior of 17-4 Precipitation Hardenable Steel Processed by Selective Laser Melting. Journal of Materials Engineering and Performance, 2014. 23(12): p. 4421-4428.

223.	Yu, J., et al., Material Properties of Ti6Al4V Parts Produced by Laser Metal Deposition. Physics Procedia, 2012. 39: p. 416-424.

224.	Dinda, G.P., L. Song, and J. Mazumder, Fabrication of Ti-6Al-4V Scaffolds by Direct Metal Deposition. Metallurgical and Materials Transactions A, 2008. 39(12): p. 2914-2922.

225.	Åkerfeldt, P., M.-L. Antti, and R. Pederson, Influence of microstructure on mechanical properties of laser metal wire-deposited Ti-6Al-4V. Materials Science and Engineering: A, 2016. 674: p. 428-437.

226.	Murr, L.E., et al., Microstructures and mechanical properties of electron beam-rapid manufactured Ti–6Al–4V biomedical prototypes compared to wrought Ti–6Al–4V. Materials Characterization, 2009. 60(2): p. 96-105.

227.	Razavi, S.M.J., et al., Porosity effect on tensile behavior of Ti-6Al-4V specimens produced by laser engineered net shaping technology. Proceedings of the Institution of Mechanical Engineers, Part C: Journal of Mechanical Engineering Science, 2018.

228.	Zhai, Y., et al., Understanding the microstructure and mechanical properties of Ti-6Al-4V and Inconel 718 alloys manufactured by Laser Engineered Net Shaping. Additive Manufacturing, 2019. 27: p. 334-344.

229.	Li, Z., et al., The microstructure evolution and tensile properties of Inconel 718 fabricated by high-deposition-rate laser directed energy deposition. Additive Manufacturing, 2020. 31.

230.	Soffel, F., et al., Interface strength and mechanical properties of Inconel 718 processed sequentially by casting, milling, and direct metal deposition. Journal of Materials Processing Technology, 2021. 291.

231.	Mazzucato, F., et al., Laser Metal Deposition of Inconel 718 Alloy and As-built Mechanical Properties Compared to Casting. Materials (Basel), 2021. 14(2).

232.	Zhu, L., Z. Xu, and Y. Gu, Effect of laser power on the microstructure and mechanical properties of heat treated Inconel 718 superalloy by laser solid forming. Journal of Alloys and Compounds, 2018. 746: p. 159-167.

233.	Kirka, M.M., et al., Mechanical behavior of post-processed Inconel 718 manufactured through the electron beam melting process. Materials Science and Engineering: A, 2017. 680: p. 338-346.

234.	Zhang, D., et al., Effect of standard heat treatment on the microstructure and mechanical properties of selective laser melting manufactured Inconel 718 superalloy. Materials Science and Engineering: A, 2015. 644: p. 32-40.

235.	Ni, M., et al., Anisotropic tensile behavior of in situ precipitation strengthened Inconel 718 fabricated by additive manufacturing. Materials Science and Engineering: A, 2017. 701: p. 344-351.

236.	Trosch, T., et al., Microstructure and mechanical properties of selective laser melted Inconel 718 compared to forging and casting. Materials Letters, 2016. 164: p. 428-431.

237.	Chlebus, E., et al., Effect of heat treatment on the microstructure and mechanical properties of Inconel 718 processed by selective laser melting. Materials Science and Engineering: A, 2015. 639: p. 647-655.

238.	Popovich, V.A., et al., Impact of heat treatment on mechanical behaviour of Inconel 718 processed with tailored microstructure by selective laser melting. Materials & Design, 2017. 131: p. 12-22.

239.	Åkerfeldt, P., R. Pederson, and M.-L. Antti, A fractographic study exploring the relationship between the low cycle fatigue and metallurgical properties of laser metal wire deposited Ti–6Al–4V. International Journal of Fatigue, 2016. 87: p. 245-256.

240.	Bantounas, I., et al., Effect of microtexture on fatigue cracking in Ti–6Al–4V. Acta Materialia, 2007. 55(16): p. 5655-5665.

241.	Caton, M.J., et al., Stress ratio effects on small fatigue crack growth in Ti–6Al–4V. International Journal of Fatigue, 2012. 38: p. 36-45.

242.	Shamsaei, N., et al., An overview of Direct Laser Deposition for additive manufacturing; Part II: Mechanical behavior, process parameter optimization and control. Additive Manufacturing, 2015. 8: p. 12-35.

243.	Yadollahi, A. and N. Shamsaei, Additive manufacturing of fatigue resistant materials: Challenges and opportunities. International Journal of Fatigue, 2017. 98: p. 14-31.

244.	Sterling, A.J., et al., Fatigue behavior and failure mechanisms of direct laser deposited Ti–6Al–4V. Materials Science and Engineering: A, 2016. 655: p. 100-112.

245.	Gordon, J., et al., Enhancement in fatigue performance of metastable austenitic stainless steel through directed energy deposition additive manufacturing. Materials & Design, 2019. 168.

246.	Wang, Y., et al., High-cycle fatigue crack initiation and propagation in laser melting deposited TC18 titanium alloy. International Journal of Minerals, Metallurgy, and Materials, 2013. 20(7): p. 665-670.

247.	Li, Z., et al., Low cycle fatigue behavior of laser melting deposited TC18 titanium alloy. Transactions of Nonferrous Metals Society of China, 2013. 23(9): p. 2591-2597.

248.	Ren, Y.M., et al., Low cycle fatigue properties of Ti-6Al-4V alloy fabricated by high-power laser directed energy deposition: Experimental and prediction. International Journal of Fatigue, 2019. 127: p. 58-73.

249.	Liu, Z., et al., Fatigue properties of Ti-6.5Al-3.5Mo-l.5Zr-0.3Si alloy produced by direct laser deposition. Materials Science and Engineering: A, 2018. 716: p. 140-149.

250.	Razavi, S.M.J., et al., Fatigue Behavior of Porous Ti-6Al-4V Made by Laser-Engineered Net Shaping. Materials (Basel), 2018. 11(2).

251.	Kumar, P. and U. Ramamurty, High cycle fatigue in selective laser melted Ti-6Al-4V. Acta Materialia, 2020. 194: p. 305-320.

252.	Wan, H.Y., et al., Effect of scanning strategy on mechanical properties of selective laser melted Inconel 718. Materials Science and Engineering: A, 2019. 753: p. 42-48.

253.	Pei, C., et al., Assessment of mechanical properties and fatigue performance of a selective laser melted nickel-base superalloy Inconel 718. Materials Science and Engineering: A, 2019. 759: p. 278-287.

254.	Simonelli, M., Y.Y. Tse, and C. Tuck, Effect of the build orientation on the mechanical properties and fracture modes of SLM Ti–6Al–4V. Materials Science and Engineering: A, 2014. 616: p. 1-11.

255.	Fatemi, A., et al., Multiaxial fatigue behavior of wrought and additive manufactured Ti-6Al-4V including surface finish effect. International Journal of Fatigue, 2017. 100: p. 347-366.

256.	Fatemi, A., et al., Torsional fatigue behavior of wrought and additive manufactured Ti-6Al-4V by powder bed fusion including surface finish effect. International Journal of Fatigue, 2017. 99: p. 187-201.

257.	Kahlin, M., H. Ansell, and J.J. Moverare, Fatigue behaviour of notched additive manufactured Ti6Al4V with as-built surfaces. International Journal of Fatigue, 2017. 101: p. 51-60.

258.	Bagehorn, S., J. Wehr, and H.J. Maier, Application of mechanical surface finishing processes for roughness reduction and fatigue improvement of additively manufactured Ti-6Al-4V parts. International Journal of Fatigue, 2017. 102: p. 135-142.

259.	Banerjee, R., et al., Microstructural evolution in laser deposited compositionally graded α/β titanium-vanadium alloys. Acta Materialia, 2003. 51(11): p. 3277-3292.

260.	Lin, X. and T.M. Yue, Phase formation and microstructure evolution in laser rapid forming of graded SS316L/Rene88DT alloy. Materials Science and Engineering: A, 2005. 402(1-2): p. 294-306.

261.	Lin, X., et al., Laser rapid forming of SS316L/Rene88DT graded material. Materials Science and Engineering: A, 2005. 391(1-2): p. 325-336.

262.	Schneider-Maunoury, C., et al., Functionally graded Ti6Al4V-Mo alloy manufactured with DED-CLAD® process. Additive Manufacturing, 2017. 17: p. 55-66.

263.	Reichardt, A., et al., Development and characterization of Ti-6Al-4V to 304L stainless steel gradient components fabricated with laser deposition additive manufacturing. 2016. 104: p. 404-413.

264.	Shah, K., et al., Parametric study of development of Inconel-steel functionally graded materials by laser direct metal deposition. Materials & Design (1980-2015), 2014. 54: p. 531-538.

265.	Hofmann, D.C., et al., Developing gradient metal alloys through radial deposition additive manufacturing. Sci Rep, 2014. 4: p. 5357.

266.	Ren, H.S., et al., Microstructure and mechanical properties of a graded structural material. Materials Science and Engineering: A, 2014. 611: p. 362-369.

267.	Carroll, B.E., et al., Functionally graded material of 304L stainless steel and inconel 625 fabricated by directed energy deposition: Characterization and thermodynamic modeling. Acta Materialia, 2016. 108: p. 46-54.

268.	Bobbio, L.D., et al., Characterization of a functionally graded material of Ti-6Al-4V to 304L stainless steel with an intermediate V section. Journal of Alloys and Compounds, 2018. 742: p. 1031-1036.

269.	Bobbio, L.D., et al., Additive manufacturing of a functionally graded material from Ti-6Al-4V to Invar: Experimental characterization and thermodynamic calculations. Acta Materialia, 2017. 127: p. 133-142.

270.	Collins, P.C., et al., Laser deposition of compositionally graded titanium–vanadium and titanium–molybdenum alloys. Materials Science and Engineering: A, 2003. 352(1-2): p. 118-128.

271.	Li, L., et al., Microstructure and mechanical properties of functionally graded TiCp/Ti6Al4V composite fabricated by laser melting deposition. Ceramics International, 2017. 43(18): p. 16638-16651.

272.	Mahamood, R.M. and E.T. Akinlabi, Laser metal deposition of functionally graded Ti6Al4V/TiC. Materials & Design, 2015. 84: p. 402-410.

273.	Zhang, Y., et al., Characterization of laser powder deposited Ti–TiC composites and functional gradient materials. Journal of Materials Processing Technology, 2008. 206(1-3): p. 438-444.

274.	Acharya, R. and S. Das, Additive Manufacturing of IN100 Superalloy Through Scanning Laser Epitaxy for Turbine Engine Hot-Section Component Repair: Process Development, Modeling, Microstructural Characterization, and Process Control. Metallurgical and Materials Transactions A, 2015. 46(9): p. 3864-3875.

275.	Leino, M., J. Pekkarinen, and R. Soukka, The Role of Laser Additive Manufacturing Methods of Metals in Repair, Refurbishment and Remanufacturing – Enabling Circular Economy. Physics Procedia, 2016. 83: p. 752-760.

276.	Chen, K., et al., Rafting-Enabled Recovery Avoids Recrystallization in 3D-Printing-Repaired Single-Crystal Superalloys. Adv Mater, 2020. 32(12): p. e1907164.

277.	Mokadem, S., et al., Laser Repair of Superalloy Single Crystals with Varying Substrate Orientations. Metallurgical and Materials Transactions A, 2007. 38(7): p. 1500-1510.

278.	Oh, W.J., et al., Repairing additive-manufactured 316L stainless steel using direct energy deposition. Optics & Laser Technology, 2019. 117: p. 6-17.

279.	Kaierle, S., et al., Single-crystal turbine blade tip repair by laser cladding and remelting. CIRP Journal of Manufacturing Science and Technology, 2017. 19: p. 196-199.

280.	Perini, M., P. Bosetti, and N. Balc, Additive manufacturing for repairing: from damage identification and modeling to DLD. Rapid Prototyping Journal, 2020. 26(5): p. 929-940.

281.	Wilson, J.M., et al., Remanufacturing of turbine blades by laser direct deposition with its energy and environmental impact analysis. Journal of Cleaner Production, 2014. 80: p. 170-178.

282.	Mudge, R.P. and N.R.J.W.J.-N.Y.-. Wald, Laser engineered net shaping advances additive manufacturing and repair. 2007. 86(1): p. 44.

283.	Sun, S., Q. Liu, and M.J.S. Brandt, Microstructure and mechanical properties of laser cladding repair of AISI 4340 steel. 2012. 1: p. 9.

284.	Li, L., Repair of directionally solidified superalloy GTD-111 by laser-engineered net shaping. Journal of Materials Science, 2006. 41(23): p. 7886-7893.

285.	Chen, H., et al., Epitaxial laser deposition of single crystal Ni-based superalloy: Variation of stray grains. Materials Characterization, 2019. 158.

Table 1 Comparison of main processing parameters and features in DED and LB-PBF processes.

| Process | DED DED DED DED |  |  |  | LB-PBF |
| --- | --- | --- | --- | --- | --- |
| Feedstock | Powder | Wire | Wire | Wire | Powder |
| Heat source | Laser | Laser | E-beam | Arc | Laser |
| Environment/ Shielding gas | Ar/N2 | Ar | Vacuum | He-Ar, Ar-CO2, Ar | Ar, N2 |
| Power (kW) | 0.2-5 | 1.5-3.5 | 1.8-3.9 | - | 0.2-2 |
| Current (A) |  |  |  | 70-160 |  |
| Scanning speed (mm/s) | 5-30 | 5-50 | 4-12 | 4-22 | 500-3000 |
| Feeding rate1 | 6-30 | 1-10 | - | 1-15 | - |
| Spot size (mm) | 1-5 | - | - | - | 0.05-0.2 |
| Layer thickness (µm) | 300-2000 | 300-2000 | - | 500-2000 | 20-90 |
| Melt pool width (µm) | 1500-3000 | - | - | - | 100-600 |
| Melt pool depth (µm) | 500-2500 | - | - | - | 200-800 |
| Surface roughness (µm) | 5-30 | - | - | 120-1000 | 12-25 |
| Ref. | [21, 43-46] | [38, 39, 47] | [40, 48, 49] | [36, 37, 41, 50, 51] | [52-59] |

- Unit for feeding rate is g/min for powder and m/min for wire.

Table 2 Easy growth directions for epitaxial growth of metals and alloys with various crystal structures [103].

| Crystal structure | Easy growth direction | Examples |
| --- | --- | --- |
| Face-centered-cubic (FCC) | <100> | Austenitic SS, Ni-based superalloys |
| Body-centered-cubic (BCC) | <100> | Ferrite SS |
| Hexagonal-close-packed (HCP) | <1010> | Ti alloys, Mg alloys |
| Body-centered-tetragonal (BCT) | <110> | Sn |

Table 3 Dislocation density in AB DED and LB-PBF components.

| Material | Process | Measurement method | Dislocation density (×1014 m-2) | Ref. |
| --- | --- | --- | --- | --- |
| 316L SS | DED | TEM | 1.0 | [149] |
| 316L SS | DED | Neutron diffraction | 2.3 | [156] |
| 304L SS | DED | EBSD | 0.34-0.43 | [136] |
| 304L SS | DED | Neutron diffraction | 2.5 ± 1.0 | [155] |
| 304L SS | DED | Neutron diffraction | 1.62 | [157] |
| Ti-6Al-4V | DED | EBSD | 26-466 | [142] |
| Inconel 625 | DED | EBSD | 0.141-0.196 | [158] |
| 316L SS | LB-PBF | TEM | 4.0 | [149] |
| 316L SS | LB-PBF | XRD | 11.4 | [159] |
| 316L SS | LB-PBF | Electron channeling contrast | 2.5 | [160] |
| 316L SS | LB-PBF | TEM | 7.2 ± 1.1 | [161] |
| 304L SS | LB-PBF | TEM | 2.0 | [162] |
| Al0.3CoCrFeNi | LB-PBF | TEM | 3.0-7.0 | [163] |

Table 4 Uniaxial tensile properties of steels fabricated by DED in comparison with that of CM counterparts.

| Materials | Geometry | P (W) | v (mm/s) | Condition |  | Phase | Direction | σY (MPa) |  | σUTS(MPa) | εf (%) | AY (%) | Aε (%) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DED |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 316L SS | Block | 800 | 10 |  | AB | - | - | 402±20 | 428±21 |  | 13.51±0.75 | - | - | [210] |
|  |  | 1000 | 13.33 |  | AB | - | - | 415±21 | 440±23 |  | 14.93±0.82 | - | - |  |
|  |  | 1150 | 16.67 |  | AB | - | - | 410±20 | 459±24 |  | 21.49±1.12 | - | - |  |
|  |  | 1450 | 20 |  | AB | - | - | 446±23 | 471±25 |  | 17.51±0.85 | - | - |  |
|  |  | 1650 | 23.33 |  | AB | - | - | 456±24 | 508±25 |  | 19.62±1.05 | - | - |  |
| 316L SS | Block | 360 | 8.5 |  | AB | γ+δ | Vertical | 410±5 | 640±20 |  | 36±4 | - | - | [23] |
|  |  | 360 | 8.5 |  | HT1 | γ | Vertical | 340±15 | 610±10 |  | 42.5±0.5 | - | - |  |
| 316L SS | Block | 900 | 15 |  | AB | γ+δ | Vertical | 469±6 | 649±2 |  | 23±3 | - | - | [28] |
| 316L SS | Block | - | - |  | AB | γ+δ | - | 470±3 | 628±7 |  | 31.2±2.2 | - | - | [29] |
| 316L SS | Block | 400 | 15 |  | AB | γ+δ | Horizontal | 576 | 776 |  | 33 | 16.84 | -39.39 | [135] |
|  |  |  |  |  |  |  | Vertical | 497 | 703 |  | 46 |  |  |  |
| 316L SS | Block | 570 | 12.5 |  | AB | γ+δ | Horizontal | 487±10 | 668±7 |  | 51.6±1.2 | 42.92 | -19.96 | [211] |
|  |  |  |  |  |  |  | Vertical | 278±9 | 569±13 |  | 61.9±3.9 |  |  |  |
| 316L SS | Block | 800 | 3 |  | AB | - | Horizontal | - | 694 |  | 40 | - | -7.5 | [212] |
|  |  |  |  |  |  |  | Vertical | - | 626 |  | 43 | - |  |  |
| 304L SS | Block | 400 | 17 |  | AB | - | Horizontal | 453±6 | 710±4 |  | 54±1 | 3.31 | -29.63 | [136] |
|  |  |  |  |  |  |  | Vertical | 438±7 | 664±5 |  | 70±2 |  |  |  |
| 304L SS | Wall | 2300 | 8.5 |  | AB | γ+δ | Horizontal | 337±29 | 609±18 |  | 48.2±2.5 | 6.82 | -17.01 | [215] |
|  |  |  |  |  |  |  | Vertical | 314±6 | 606±13 |  | 56.4±5.8 |  |  |  |
|  | Wall | 4000 | 10.6 |  | AB | γ+δ | Horizontal | 277±27 | 581±20 |  | 41.8±3.5 | 1.08 | -20.81 |  |
|  |  |  |  |  |  |  | Vertical | 274±7 | 560±12 |  | 50.5±6.7 |  |  |  |
| 17-4 PH | Block | 685 | 10 |  | AB | γ+M | Horizontal | 758±19 | 1129±5 |  | 14.1±0.3 | 21.50 | 73.05 | [168] |
|  |  |  |  |  |  |  | Vertical | 595±14 | 918±13 |  | 3.8±1.3 |  |  |  |
| 17-4 PH | Block | 800 | 10 |  | AB | γ+M | Horizontal | 574±16 | 1005±5 |  | 19.4±1.4 | - | - | [167] |
|  |  |  |  |  | HT2 | γ+M |  | 856±10 | 1070±20 |  | 17.3±1.3 |  |  |  |
| 17-4 PH | Block | - | 6.2 |  | AB | γ+M | Horizontal | 842±65 | 1009±55 |  | 11.6±0.3 | 12.35 | -5.17 | [220] |
|  |  |  |  |  |  |  | Vertical | 738±30 | 979±13 |  | 12.2±0.7 |  |  |  |
|  |  |  |  |  | HT3 | - | Horizontal | 815±24 | 1000±5 |  | 12.8±0.2 | -1.47 | 3.13 |  |
|  |  |  |  |  |  |  | Vertical | 827±4 | 1006±6 |  | 12.4±0.4 |  |  |  |
|  |  |  |  |  | HT4 | - | Horizontal | 1140±57 | 1293±32 |  | 8.2±0.3 | 7.11 | 20.73 |  |
|  |  |  |  |  |  |  | Vertical | 1059±9 | 1124±5 |  | 6.5±0.3 |  |  |  |
|  |  |  |  |  | HT5 | - | Horizontal | 1225±36 | 1353±6 |  | 13.8±1.4 | -0.73 | 0.00 |  |
|  |  |  |  |  |  |  | Vertical | 1234±33 | 1351±11 |  | 13.8±0.5 |  |  |  |
| CM |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 316L SS | Block | - | - |  | As-cast | γ | - | 200±30 | 450±25 |  | 45±4 | - | - | [213] |
| 316L SS | Block | - | - |  | Wrought | γ | - | 220-270 | 520-680 |  | 40-45 | - | - | [214] |
| 304L SS | Block | - | - |  | Annealed | γ | - | 265±9 | 722±14 |  | 62.3±2.6 | - | - | [215] |
| 17-4 PH | Block | - | - |  | Wrought (HT6) | M |  | 992 | 1018 |  | 13.4 | - | - | [221] |

- Homogenizing heat treatment: 1150 °C for 2 h

- ST: 1040 °C for 1 h followed by AT: 550 °C for 2 h

- ST: 1040 °C for 0.5 h

- AT: 480 °C for 1 h

- ST: 1040 °C for 0.5 h followed by AT: 480 °C for 1 h

- ST: 1038 °C for 0.5 h

Table 5 Uniaxial tensile properties of Ti-6Al-4V fabricated by DED in comparison with that of CM counterparts.

| Materials | Geometry | P (W) | v (mm/s) | Condition | Phase | Direction | σY (MPa) |  | σUTS (MPa) | εf(%) | AY (%) | Aε (%) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DED |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Ti-6Al-4V | Block | - | - | AB | α' | Horizontal | 950±2 | 1025±10 |  | 12±1 | 0.00 | 0.00- | [178] |
|  |  | - | - |  |  | Vertical | 950±2 | 1025±2 |  | 5±1 |  |  |  |
| Ti-6Al-4V | Block | 2000 | 10.6 | AB | α+β | Horizontal | 1015±12 | 1118±10 |  | 12±3 | 9.06 | 66.67 | [179] |
|  |  |  |  |  |  | Vertical | 923±25 | 1042±29 |  | 20±3 |  |  |  |
|  |  |  |  | AB |  | Horizontal | 988±29 | 1087±31 |  | 20±3 | 6.48 | -10.00 |  |
|  |  |  |  |  |  | Vertical | 924±26 | 1031±29 |  | 22±4 |  |  |  |
|  |  |  |  | AB |  | Horizontal | 994±33 | 1104±24 |  | 12±2 | 3.52 | -16.67 |  |
|  |  |  |  |  |  | Vertical | 959±29 | 1072±29 |  | 14±4 | - |  |  |
|  |  |  |  | AB |  | Horizontal | 973±25 | 1076±25 |  | 20±3 | 3.60 | -15.00 |  |
|  |  |  |  |  |  | Vertical | 938±22 | 1048±23 |  | 23±3 |  |  |  |
| Ti-6Al-4V | Block | 470 | 16.67 | AB | α' | Horizontal | 976±24 | 1099±2 |  | 4.9±0.1 | - | - | [223] |
| Ti-6Al-4V | Block | 330 | 10 | AB | α' | Horizontal | 1005 | 1103 |  | 4 | - | - | [180] |
|  |  | 780 | 13.33 | AB | α'+α | Horizontal | 990 | 1042 |  | 7 | - | - |  |
| Ti-6Al-4V | Block | 300 | 0.61 | AB | α+β, GB α | - | 1105±19 | 1163±22 |  | 4±1 | - | - | [224] |
| Ti-6Al-4V | Wall | 2000 | 10.6 | AB | α+β, GB α | Horizontal | 960±26 | 1063±20 |  | 10.9±1.4 | 1.56 | -33.03 | [114] |
|  |  |  |  |  |  | Vertical | 945±13 | 1041±12 |  | 14.5±1.2 |  |  |  |
| Ti-6Al-4V | Wall | 2000 | 10.6 | AB | α+β | Horizontal | 959±32 | 1077±33 |  | 18±2 | 6.67 | 0.00 | [179] |
|  |  |  |  |  |  | Vertical | 895±19 | 1012±20 |  | 18±2 |  |  |  |
|  |  |  |  |  |  | Horizontal | 947±29 | 1059±18 |  | 18±4 | 1.48 | 5.56 |  |
|  |  |  |  |  |  | Vertical | 933±18 | 1047±18 |  | 17±4 |  |  |  |
|  |  |  |  |  |  | Horizontal | 923±15 | 1043±10 |  | 19±5 | 2.38 | 21.05 |  |
|  |  | - | - |  |  | Vertical | 901±11 | 1024±13 |  | 15±5 |  |  |  |
|  |  | - | - |  |  | Horizontal | 910±17 | 1035±18 |  | 13±2 | 4.29 | -46.15 |  |
|  |  |  |  |  |  | Vertical | 871±19 | 995±18 |  | 19±3 |  |  |  |
| Ti-6Al-4V | Block | 330 | 10 | HT1 | α+β | Horizontal | 1000 | 1073 |  | 9 | - | - | [180] |
|  |  | 780 | 13.33 | HT1 | α+β | Horizontal | 991 | 1044 |  | 10 | - | - |  |
| Ti-6Al-4V | Block | 300 | 0.61 | HT2 | α+β, GB α | - | 975±15 | 1053±18 |  | 7.5±1 |  |  | [224] |
|  |  |  |  | HT3 | α+β, GB α | - | 959±12 | 1045±16 |  | 10.5±1 |  |  |  |
|  |  |  |  | HT2 | α+β, GB α | - | 931±16 | 1002±19 |  | 6.5±1 |  |  |  |
|  |  |  |  | HT3 | α+β, GB α | - | 900±14 | 951±15 |  | 7.5±1 |  |  |  |
| Ti-6Al-4V | Block | - | 10 | HT4 | α+β, GB α | Horizontal | 804 | 920 |  | 12.1 | 1.87 | -33.06 | [225] |
|  |  |  |  |  |  | Vertical | 789 | 884 |  | 16.1 |  |  |  |
| Ti-6Al-4V | Wall | 300 | 4 | HT5 | α+β, GB α | Horizontal | 1020 | 1190 |  | 4.3 | 11.76 | -230.23 | [16] |
|  |  |  |  |  |  | Vertical | 900 | 1050 |  | 14.2 |  |  |  |
| CM |  | - | - |  |  |  |  |  |  |  |  |  |  |
| Ti-6Al-4V | Block | - | - | Wrought |  | - | 962 | 1008 |  | 19 | - | - | [226] |

- 760±4 °C for 1 h.

- 950 for 1h, air cooling.

- 950 °C for 1h, furnace cooling.

- 704 °C for 2h.

- 560 °C for 2h

Table 6 Uniaxial tensile properties of Inconel 718 fabricated by DED in comparison with that of CM counterparts.

| Materials | Geometry | P (W) | v (mm/s) | Condition |  | Direction | σY (MPa) | σUTS (MPa) | εf (%) | AY (%) | Aε (%) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DED |  |  |  |  |  |  |  |  |  |  |  |  |
| Inconel 718 | Block | 2350 | 8 |  | AB | - | 590 | 845 | 11 | - | - | [198] |
| Inconel 718 | Block | - | - |  | AB | Horizontal | 650 | 1000 | - | - | - | [190] |
| Inconel 718 | Block | 450 | 8.33 |  | AB | Horizontal | 715 | 941 | 17.6 | - | - | [228] |
|  |  | 840 | 10.4 |  | AB | Horizontal | 668 | 960 | 21.6 | - | - |  |
| Inconel 718 | Block | 4000 | 26.67 |  | AB | Horizontal | 745 | 1051 | 31.2 | - | - | [229] |
|  |  |  |  |  |  | Horizontal | 752 | 1074 | 22.5 | - | - |  |
|  |  |  |  |  |  | Horizontal | 465 | 822 | 33.9 | - | - |  |
| Inconel 718 | Block | 725-1000 | 3.33-5.55 |  | AB | Horizontal | 561±4 | 909±1 | 31.3±0.8 | 7.31 | 11.82 | [230] |
|  |  |  |  |  |  | Vertical | 520±2 | 932±5 | 27.6±1.0 |  |  |  |
| Inconel 718 | Block | 300 | - |  | AB | - | 557±33 | 838±6 | 50.4±3.9 | - | - | [231] |
|  |  | 400 | - |  | AB | - | 554±42 | 869±15 | 44.7±2.2 | - | - |  |
| Inconel 718 | Block | 2500 | 10 |  | AB | Vertical | 544 | 879 | 43 | - | - | [196] |
| Inconel 718 | Block | 2350 | 8 |  | HT1 | - | 1133 | 1240 | 9 | - | - | [198] |
|  |  |  |  |  | HT1 | - | 1170 | 1360 | 18 | - | - |  |
| Inconel 718 | Block | - | - |  | HT2 | Horizontal | 1257 | 1436 | - | - | - | [190] |
| Inconel 718 | Block |  |  |  | HT3 | Vertical | 1084 | 1333 | 8.4 |  |  |  |
|  |  | - | - |  | HT2 | Vertical | 1007 | 1221 | 16 | - | - |  |
|  |  |  |  |  | HT1 | Vertical | 949 | 1194 | 19.9 | - | - |  |
| Inconel 718 | Block | 450 | 8.33 |  | HT4 | Horizontal | 1120 | 1365 | 7 | - | - | [228] |
|  |  | 840 | 10.4 |  | HT4 | Horizontal | 1040 | 1318 | 9.5 | - | - |  |
| Inconel 718 | Block | 2500 | 10 |  | HT3 | Vertical | 1035 | 1294 | 10.5 | - | - | [196] |
|  |  |  |  |  | HT2 | Vertical | 1060 | 1290 | 15.4 | - | - |  |
|  |  |  |  |  | HT1 | Vertical | 1114 | 1316 | 26.1 | - | - |  |
| Inconel 718 | Block | 1250 | 16.67 |  | HT5 | Vertical | 313 | 687 | 54 | - | - | [232] |
|  |  |  |  |  | HT1 | Vertical | 1061 | 1278 | 19 | - | - |  |
|  |  | 1300 | 16.67 |  | HT5 | Vertical | 328 | 726 | 57 | - | - |  |
|  |  |  |  |  | HT1 | Vertical | 1093 | 1307 | 17.5 | - | - |  |
|  |  | 1350 | 16.67 |  | HT5 | Vertical | 340 | 756 | 61 | - | - |  |
|  |  |  |  |  | HT1 | Vertical | 1129 | 1342 | 16 | - | - |  |
|  |  | 1400 | 16.67 |  | HT5 | Vertical | 325 | 718 | 55 | - | - |  |
|  |  |  |  |  | HT1 | Vertical | 1077 | 1298 | 18 | - | - |  |
| CM |  | - | - |  |  |  |  |  |  |  |  |  |
| Inconel 718 | Block |  |  |  | As-cast | - | 758 | 802 | 5 | - | - | [233] |
| Inconel 718 | Block | - | - |  | Wrought | - | 1100 | 1340 | 12 | - | - | [198] |

Homogenization treatment: 1093 ± 14 °C, 1 to 2 h, air cooling/ water cooling; ST: 954 to 982°C, >1 h, air cooling/water cooling; AT: 718± 8°C, 8 h, furnace cooling to 621± 8 °C, 10 h, air cooling/ water cooling

- HT1: HSAT

- HT2: SAT

- HT3: AT

- HT4: 732 °C, 4 h, furnace cooling

- HT5: Homogenization treatment

Table 7 Mechanical properties of components in undamaged and DED-repaired conditions.

| Materials | Condition | σY (MPa) | σUTS (MPa) | εf (%) | Ref. |
| --- | --- | --- | --- | --- | --- |
| 316L SS | CM (Hot-annealed) | 297 | 737 | 64 | [278] |
|  | DED-repaired1 | 297 | 698 | 55 |  |
|  | DED-repaired2 | 300 | 608 | 26 |  |
|  | DED-repaired3 | 270 | 381 | 6 |  |
|  | LB-PBF (AB) | 529 | 709 | 44 |  |
|  | DED-repaired1 | 526 | 689 | 42 |  |
|  | DED-repaired2 | 485 | 641 | 26 |  |
|  | DED-repaired3 | 443 | 490 | 4 |  |
| Inconel 625 | CM (Annealed) | 403 | 841 | 30 | [281] |
|  | DED (AB) | 487 | 815 | 69 |  |
|  | DED-repaired | 482 | 793 | 56 |  |
| Al-12Si | CM | 521 | 545 | - | [13] |
|  | DED-repaired | 481 | 525 | - |  |

- Repairing groove depth: 0.5 mm

- Repairing groove depth: 1.0 mm

- Repairing groove depth: 2.0 mm