Dual phase AlxCoCrFeNi with trade off strength/ductile developed by high-throughput laser powder-bed fusion technology

Chaoyang Guo a, Baicheng Zhang a, b *, Pei Wang c, Upadrasta Ramamurty d, Xuanhui Qu a,b

a Beijing Advanced Innovation Center Materials Genome Engineering, Advanced Material & Technology Institute, University of Science and Technology Beijing, Beijing 100083, China

b Beijing Laboratory of Metallic Materials and Processing for Modern Transportation, Beijing 100083, China

c IMRE - Institute of Materials Research and Engineering, 2 Fusionopolis Way, Innovis, #08-03, Singapore 138634, Singapore

d School of Mechanical & Aerospace Engineering,

Nanyang Technological University

*Corresponding Author, E-mail address: zhangbc@ustb.edu.cn

Abstract

High entropy alloys (HEAs) exhibit multiple excellent properties because its unique design and atom structure. However, the exploring of its vast compositional space composition and complex microstructure is a grand challenge. A new self-developed high-throughput laser powder bed fusion (LPBF) system is proposed for large-scale microstructurally and compositionally graded HEAs preparation. In this study, an AlxCoCrFeNi (0<x<20) compositionally graded alloy component is prepared. The phase selection, texture and mechanical properties evolution are systematically studied. The crystal-structures of printed AlxCoCrFeNi HEAs were gradually transformed from FCCFCC+BCCBCC, with increasing Al content, accompanied with an increase in microhardness and tensile strength. Interestingly, compared to traditional HEAs preparation techniques, the phase transition interval from FCC to BCC of laser processed AlxCoCrFeNi is significantly advanced and narrowed, due to the ultrafast cooling rate and thermal cycles during LPBF. Moreover, the dual-phase region is found at Al0.52CoCrFeNi with BCC/FCC layer-wise distribution. Distinguish with the significant <001> orientation from FCC or BCC regions from printed AlxCoCrFeNi component, the dual-phase structure shows a fine equiaxed grain without obvious texture. Tensile results demonstrate that the as-printed dual-phase alloy maintains 748 MPa tensile strength with about 22.8% elongation. The trade-off in strength and ductility is attributed to the unique coupled eutectic-like distribution of the ductile FCC and brittle BCC phases with fine densely arranged grains. At last, the fundamental mechanisms for the advancement of phase transformation endpoints in dual-phase HEAs and cracking behavior with high aluminum content under nonequilibrium conditions were analyzed.

Keywords: LPBF; HEAs; High throughput; Microstructure; Mechanical property.

1. Introduction

High-entropy alloys (HEAs) as entropy-driven multi-component alloys with simple phase solid

solution structures, containing five or more major elements of equal or unequal atomic percentages, first developed by Yeh[1] and Cantor[2] in 2004. The advanced design concept subverts the traditional metallurgy and phase equilibrium theory enables to provide outstanding material properties: such as high strength and tenacity at cryogenic temperatures[3][4], high fatigue resistance[5][6], high-temperature oxidation resistance[7], corrosion resistance[8], etc. As study in-depth, the definition range of HEA extended, the phase structure is not only restricted to single-phase solid solution (SPSS), the secondary precipitation[12], eutectic structure[13], even ceramic strengthen phase[14] were included in HEA system. It is worth to notice that the composition of HEAs is a vast, multidimensional space over phase structure or properties which is beyond traditional alloy preparation or characterization method. Moreover, the traditional phase and properties predication rules such as Hume-Rothery rules has been proved not applicable for HEAs due to the unique atomic level structure[15]. To date, the main challenge and center of HEA research is attributed to: phase selection behaviors and the corresponding performance optimization under multi-element combination [16].

As most studied HEAs system, the phase selection behavior of AlxCoCrFeNi alloy is widely reported.[16][17]. The mechanism of phase transformation from FCC to BCC is attributed to the Al content increase as BCC phase stabilizer[1][18]. However, most current published work of HEAs phase selection and stability only report under equilibrium state with a limited set of mechanical properties [21-25]. As study in-depth, authors found that the phase structure transformation of HEAs is found not only influenced by the composition, but also by cooling rate of technology process. For instance, the composition variation interval (at.%) for Al in the dual phase region is about 9-18% for casting [21], 11-18% for arc melting [18] and 10-15% for laser metal deposition [26] in the AlxCoCrFeNi HEAs system. Obviously, the law applied for HEAs phase selection under equilibrium is not applicable for that under non-equilibrium. At present, little work has been made on phase transformation behavior and mechanical properties optimization for HEAs under non-equilibrium, and, consequently, guidance for future development of HEAs processing technique under different cooling rate is very much lacking in fundamental principles and design potential. One strategy to study a large number of alloys in a consistent manner is combinatorial synthesis paired with high- throughput characterization. Such methods have been proven powerful across a wide range of materials classes and scientific questions.

Motivated by the above concerns, a new high-through system based on laser powder-bed fusion with rapid cooling rate on the order of 108 K/s is designed for HEAs alloy investigation. Distinct to high-throughput laser deposition currently used more widely in the MAM field [26][33-34], the new powder distribution strategy followed by this LPBF system allows the preparation of compositionally varied, smooth gradients, high precision and large scale compositionally graded HEAs for microstructural analysis and corresponding tensile testing. AlxCoCrFeNi was selected as the candidate system for compositional gradient HEAs samples preparation. The composition, structure and morphology of the as-printed gradient samples were characterized using inductively coupled plasma emission spectroscopy (ICP-OES), X-ray diffraction (XRD), scanning electron microscopy (SEM), Electron backscatter diffraction (EBSD) and transmission electron microscopy (TEM). We discovered the dual-phase structure and pinpointed the composition during preparation and characterization. The resulting data subsequently are analyzed for correlations with equilibrium and non-equilibrium condition suggested phase formation and selection rules. In addition, systematically study the effect law of cooling rate on the phase transformation of HEAs in the non-equilibrium state and the reasons of cracks with high Al content. The deeper objective of this work is to initially explore this system's utility in quickly screening the complex components and phase space of HEAs, and then provide a feasible scheme for understanding the complex performance space of HEAs to quickly obtain the corresponding component-structure-performance database.

2.	Materials and experiment methods

2.1 Component gradient HEAs LPBF systems

A self-developed high-throughput laser powder bed fusion (LPBF) system was used to fabricate the AlxCoCrFeNi specimens with continuous gradients. Through the special design of the powder storage tank, powder mixing and powder laying mechanism of the selected area laser melting equipment, the large-size continuous composition gradient alloy is manufactured horizontally by using the powder layer laid according to the required gradient ratio. The system has been used for the development of relevant functional gradient materials, demonstrating reliability in achieving composition classification [35].

In this system, printable build volume of 120 x 120 x 150 mm3 (length × width × height) can be printed in an argon atmosphere, equipped with a fibre optic laser source, its maximum power and scanning speed are 500W and 7m/s respectively, and the laser spot diameter is 30um. Using orthogonal design of experiments to optimize printing parameters for CoCrFeNi/AlCoCrFeNi. The hatch distance and layer thickness are fixed at 120 μm and 50 μm respectively, and parameters are optimized by varying the laser power and scanning speed. At a combination of laser power and speed of 300W and 714mm/s respectively, CoCrFeNi/AlCoCrFeNi densities are optimally traded off.

A stainless steel substrate was used in printing process. Two kinds of specimen with different dimensions were designed and built in Magics software. Fig.1(a) depicts the corresponding relationship between the two printing. Fig.1(b) and (c) is an image of the AlxCoCrFeNi specimens printed for metallographic characterization and tensile testing respectively. Rectangular specimens with 110 x 10 x 6 mm3 for metallographic characterization were first successfully printed.

Fig. 1. (a) Schema of the continuous component gradient HEAs LPBF system developed in this study. (b) and (c) As-printed samples image.

2.2 Feedstock powder material

Isoatomic CoCrFeNi and AlCoCrFeNi alloy powders prepared by the atomization method (Beijing Ruybon new material technology Co., Ltd.) were selected. The compositions of two feedstock powders are shown in Table 1, standard Hall flow rate test result of 18.5s. The particle size distribution of the used powders ranges from 15 to 53µm with spherical or sub-spherical shape, and the particle morphologies as shown in Fig.2.

Fig. 2. SEM images of feedstock powders morphology (a) CoCrFeNi, (b) AlCoCrFeNi.

Table 1 Chemical compositions of CoCrFeNi and AlCoCrFeNi powders

|  | Unit | Al | Co | Cr | Fe | Ni |
| --- | --- | --- | --- | --- | --- | --- |
| CoCrFeNi | wt.% | 0 | 26.23 | 23.36 | 25.28 | Bal. |
|  | at.% | 0 | 25.01 | 25.37 | 25.50 | Bal. |
| AlCoCrFeNi | wt.% | 10.71 | Bal. | 20.37 | 21.56 | 22.85 |
|  | at.% | 20.05 | Bal. | 19.79 | 19.50 | 19.66 |

2.3 Microstructure and property characterization

In order to demonstrate the continuity of the Al content variations, the composition at 11 positions was quantified using ICP (Inductive Coupled Plasma Emission Spectrometer). To determine the phase transition progression, the phase at each position was characterized using Bruker D8Focus X-ray diffractometers with Cu target tubes and scanning steps of 0.02o with 6o/min. The samples were sequentially ground, polished and etched by Wang aqueous solutions (Erosion was carried out in a 3:1 ratio of HCL and HNO3). Porosity of printed sample was obtained from the optical image based on image-pro software. The microstructure and texture were analyzed by SEM (SU8100) and EBSD (FEI Quanta 650F). The sample with dual phase region was further observed by TEM (FEI Talos F200X). Microhardness was measured with standard Vickers microhardness tester, using 100 g load for 15 seconds, striking 30 hardness points in one-dimensional gradient direction of the sample, averaged three times near each position. Tensile tests are performed on a computer-controlled material testing systems servo-hydraulic testing machines following ASTM-E8.

3. Results and discussions

3.1 Relative density and composition distribution

Fig.3(a) presents the variation of the relative densities along the one-dimensional gradient obtained by the photo microscopy method, which generally remain above 99.5%, but the high Al section, i.e. 95 mm, rapidly decreases to 97% due to cracking generation. The element composition evolution obtained from ICP analysis along gradient direction is shown in Fig.3. At the position 5 to 105 mm, it can be observed that the variation interval for all four elements Co, Cr, Fe and Ni is less than 5 at.%, nearly uniform distribution, Al content showed a one-dimensional linear increasing trend with a composition interval of 1 to 16 at.%. The Al content of each location interval were lower than theoretically expected, but in line with design expectations. The deviations from expectations can be attributed to the low-melting point Al element evaporation loss during the laser irradiation [36].

Fig. 3. Relative density (a) and chemical composition distributions (b) along the gradient direction in the as-printed AlxCoCrFeNi compositionally HEAs

3.2 Phase transformation behavior

Fig.4 (a) shows the XRD patterns from LPBF printed AlxCoCrFeNi with variation of Al content along a one-dimensional gradient. FCC phase with (111), (200) and (220) peaks can be found in range from Al0.04 to Al0.61 (mol, herein after Al content referred to Alx). While BCC phase with (110), (211) and (200) peaks can be found in range from Al0.61 to Al0.75. Ordered B2 (100) diffraction peaks can be identified at Al0.7. Fig.2 (b) and (c) present shift behavior of (200) peak from FCC phase and (211) peak from BCC phase. It is obvious that the both peaks shift toward low-angle with Al content increasing, which illustrates that the lattice constant of both FCC and BCC phases in AlxCoCrFeNi gradually increase doping by large atomic radius of Al atoms. Meanwhile, the BCC (211) peak intensity increases accompanied by the FCC (200) peak intensity reduction, suggesting that the BCC phase increases in crystallinity and the grains gradually become long-range ordered, results that the BCC phase gradually replaces the FCC phase as the matrix phase with increasing Al content. In order to quantify the phase variation, FCC/BCC phases proportions are calculated based on XRD pattern fitting and EBSD mapping, as shown in Fig. 4 (d). Three phase composition regions can be drawn as: (I) FCC single phase with Al0.04 to Al0.28 where BCC proportion is below 5 wt.%; (II) FCC/BCC dual phase from Al0.37 to Al0.61 in where Al0.52 presents an approximately equal proportion; (III) BCC single phase from Al0.7 to Al0.75 where FCC proportion is below 5 wt.%.

Fig. 4 (a) XRD diffraction patterns of printed AlxCoCrFeNi with variation of Al content; (b) magnification peak shift behavior for FCC (200) peak at 2Theta of 64~67°; (c) magnification peak shift behavior for FCC (220) peak at 2Theta of 64~67°; (d) Phase proportions for each composition interval of AlxCoCrFeNi obtained by XRD fitting and EBSD mapping.

At present, valence electron concentration (VEC) is widely accepted and used for phase transformations behavior prediction of HEAs [20]:

VEC=i=1nCi∙VECi

Where Ci and VECi are the molar fraction and VEC of composing element i.

In generally, the statistical results show that the variation trend of VEC and phase selection is consistent with previous studies: VEC decreases linearly with increasing Al content, resulting HEAs with higher VEC favors FCC over BCC [29]. However, the commonly used threshold criterion (FCC favors VEC > 8.0, BCC favors VEC < 6.8) is found not applicable in non-equilibrium processes. Fig.5 compares phase composition ranges of AlxCoCrFeNi system in VEC curves obtained from this study and other various HEAs preparation. The VEC threshold regions of FCC/BCC dual-phase in all HEAs processes were significantly narrower (8.0 to 7.3) than theory (8.0 to 6.87). Corresponding VEC threshold for single FCC phase in AC and VAM process are below 8.0, while that for single BCC phase in all processes are far above 6.87 (about 7.3). Furthermore, the VEC threshold variation for phase selection is found to be highly relevant to the HEAs process. Based on previous results, the cooling rate of the processes can be order as following: SLM (106~108 k/s) >LMD (Laser metal deposition, 103~105k/s) >VAM (Vacuum arc remelting, 100 k/s) >AC (As cast, 10~100 k/s). According to the curves distribution followed cooling rate of process, high cooling rate leads to BCC phase generated more advance (with less Al content).

Fig.5. Variation of valence electron concentration (VEC) as a function of Al content in AlxCoCrFeNi.(AC: As-cast; VAR: Vacuum arc re-melting; LMD: Laser metal deposition)

As Al content increase in AlxCoCrFeNi system, the addition of large atomic radius Al results in  lattice volume strain. Once the strain exceeds the critical value. the stable state of crystals was disrupted. The atoms tend to carry out low-density stacking for distortion energy release, thus the BCC phase nucleation barrier can be passed, the phase transformation was initiated from FCC to BCC[37][38]. At low cooling rate of solidification with equilibrium, diffusion elements are easy to pass through the lattice due to strongly interdiffusion and relatively sufficient time, the Gibbs energy in the alloy system decreases, allowing wide distribution of the different phase components, especially Al. Hence numerous Al components are required for complete suppression of FCC phase dependent growth behavior [39][40]. The printing of gradient components by LPBF is a non-equilibrium process, ultra-high cooling rate can lead to significant dynamic supercooling. Therefore, the ultrafast solidification cooling rate strongly suppresses the interdiffusion behavior of each component, the diffusion time is seriously insufficient, result the migration of grain boundary/phase boundary was hindered. The strong temperature gradient effect not only extend the solid solubility of Al, but also interrupts the elements diffusion. Although the nucleation and growth rate of FCC phase also increase relatively, the dominant expansion rate of BCC phase in the competitive growth would be much larger than that of FCC with the gradual increase of Al content, which would rapidly break the balance of the two interdependent growths. The result is that BCC can quickly replace FCC as the matrix phase without excessive Al addition, causing the biphasic composition interval to be narrower in the non-equilibrium condition of high-energy beams.

3.3 Microstructure and texture evolution

To investigate the microstructural evolution induced by the addition of Al, the microscopic and sub-microscopic morphology of the LPBFed AlxCoCrFeNi HEAs is characterized in Fig.6(a) and Fig.6(b) respectively. The interior of the molten pool is typical printed columnar crystal structure, column diameter is about 500nm, size is about 20~30um. As the Al content increases the size of columnar structure decreased and the arrangement became more dense. Minor honeycombed appear corresponding to BCC phases, mainly distributed around the melt pool boundary. However, with the increase of Al content in the range of Al0.28-Al0.52, microstructure transformed obviously, large areas of typical spinodle decomposition of woven structures are observed, similar to eutectic organization according to the literature[18][21], and the cylinder size is reduced to about 5um. Al0.52 exhibited spindle weave structure formed during a spinodal decomposition, overall microstructure comprises FCC and BCC dual-phase grains with messy distribution. The spinodle decomposition structure disappears and some recovery of the cylinder dimensions can be observed in Al0.75 section. According to the results of XRD and EBSD, the matrix phase transforms into BCC phase, and minor ordered BCC phase appears with island-like shape. The corresponding trends in average sub-grains size values with Al content have been demonstrated in Fig.6(b), the average sub-grains size of FCC phase gradually decreases from about 35um (Al0.04) to 11um (Al0.52), subsequently increase to 19um at Al0.75. General agreement is that the continuous addition of large atomic size Al will cause a strong lattice distortion enhancement effect in CoCrFeNi matrix alloy, excess volume favours diffusion, the higher the Al content, the greater the surface diffusion coefficient[1][38][41][42][43]. Therefore, the increased lattice distortion and residual stresses caused by the LPBF thermal gradient will contribute to the generation numerous defects, such as vacancies, stacking faults and non-equilibrium phase boundaries, more nucleation sites are provided for grains or subgrains.

Fig. 6. Microstructures(a) and sub-microstructures(b) along gradient direction in the LPBF printed AlxCoCrFeNi alloys.

Fig.7(a) and(b) illustrates the mapping and IPF images of AlxCoCrFeNi with Al0.04, Al0.28, Al0.37, Al0.52, Al0.61, Al0.75, respectively. The phase transformation trend of printed dual-phase alloys with Al composition was visually demonstrated by EBSD-mapping, and single-phase and dual-phase alloys were distinguished by 5 wt.%. The composition range of Al0.37-Al0.61 belongs to FCC/BCC dual-phase alloy. The uniform proportion of dual phase is observed in Al0.52, showing alternating hierarchical distribution along the gradient direction. It is confirmed that the spindle weave structure observed in Fig.6 (a) is FCC phase. Interestingly, it can be expected that the BCC phase initiates nucleation at the melt pool boundary during LPBF printing process, and then migrates nearby to gradually replace the FCC phase as the matrix phase. The initial monolayers of FCC and BCC form as fine equiaxed grains, which are controlled by global heat flow directions and steep temperature gradients, resulting the grow epitaxially as columnar grains in the <001> direction which intersecting multiple melt pools parallel to the build direction [30]. However, the dual-phase region IPF of the Al0.52 alloy did not reveal the strong grain preference orientation that was observed in the Al0.04, Al0.28 and Al0.75 single-phase regions. Fig.7(c) lists the corresponding crystal texture index ((CTI) shows that the FCC and BCC in the dual-phase region to be 3.76 and 2.62 respectively, which are lower compared to the single-phase region along the build direction, suggesting weakened texture and suppressed preferential solidification in dual-phase region.

Fig. 7. The phase mapping(a), IPF maps(b) and pole figures(c) of printed AlxCoCrFeNi HEAs along the gradient direction

3.3 Dual-phase section analysis

To further investigate the structure of dual-phase, a detailed composition and microstructure analysis of Al0.52 was carried out using SEM-EDS and TEM, as shown in Fig.8. Fig.8(a-f) presents the EDS results in the Al0.52 section, EDS line and maps confirm the enrichment of Al at the melt pool boundary, and the woven fibre structure is Al-poor with messy distribution and belongs to the FCC phase. TEM results in Fig. 8 (g-o) displaying the structural and composition distribution of the dual phase micro-region, distinct FCC and BCC(B2) slat structures were clearly observed through different contrasts (bright and dark, respectively). According to calibration of SAED from Fig.8(h) and (j), the bright area is corresponding to BCC phase, and dark area is corresponding to FCC phase, between both can observed obvious severely distorted interface. Such pinning effect between phase boundaries can significantly enhance the strain hardening or dislocation accumulation ability in alloys to achieve excellent strength- ductility synergy [44]. It can be found that the crystalline band axis of BCC [001] with finer spots around the diffraction spot, complicated spot pattern, may occur as a secondary diffraction effect. Fine diffraction spots are probably super-dotted formations of ordered solid solution, low content, likely ordered BCC phase (namely B2, crystal plane spacing and pinch angle calculations remain essentially identical to BCC phase). Fig.8(j) shows regular parallel bright and dark equal-thickness stripes. Crystal columns in the stacking fault region are split into two parts by stacking fault facets, both sides show identical crystal orientations. Extensive occurrence of stacking fault is related to LPBF's excessively high cooling rate, strong thermal gradients during solidification make local regions within the crystal have a wrong stacking order of atomic facets, resulting in elevated stacking fault energy [45]. Fig.8(k) shows typically deformed dislocation, distributed with disordered dislocation lines, its formation is related to the massive aggregation of supersaturated vacancies generated within the crystal during faster solidification at high temperatures. This typical strain field lining is produced by point distortions near the dislocation lines. Figure 8 (l-o) displays the composition distribution of the dual-phase microregion through TEM-EDS maps (and the composition point measurements of the two phases are given in Table 2). apparent chemical gradient can be observed between the dual phases, confirming the FCC phase region possesses a higher Fe and Co composition, while Al is enriched in the BCC phase region and the boundary between dual phases, which is in agreement with the SEM-EDS Al segregation at the melt pool boundary.

Fig.8 (a-f) SEM-EDS acquired components in different characteristic phase regions in the Al0.52 alloy; Printed TEM bright field image of dual-phase at position Al0.52 (g, l) and SAED pattern (b) (c) and (m) (n); (d) TEM bright field displaying stacking layer dislocations; (e) TEM bright field displaying deformation dislocations and dislocation density; (l-o) TEM-mapping results of dual-phase region.

Table 2 The TEM-EDS point composition results for the red and blue regions in Fig. 8(f)

| Element(at.%) | Al | Cr | Fe | Co | Ni |
| --- | --- | --- | --- | --- | --- |
| Red(FCC) | 9.20 | 22.25 | 23.38 | 23.53 | 21.65 |
| Blue(BCC/B2) | 11.31 | 22.20 | 21.92 | 22.57 | 22.00 |

Further displaying the mapping and IPF of Al0.52 dual-phase alloys in Fig.10, it is observed that unique equiaxed crystal-like distribution along the build direction and the two phases alternate regularly in different regions of the melt pool, where the strong phase transformation dominated by Al causes the equiaxed grains in each layer to have difficulty in epitaxial growth layer by layer. Combined with the surface convexity phenomenon of FCC phase in Al  dual-phase alloy observed in Fig.6(a), it is inferred that the transformation between FCC/BCC phase is similar to the martensitic transformation in traditional steel[46]. During the phase transformation, the BCC phase is formed on the specific crystal plane of FCC, and the two maintain a certain coherent relationship, that is, the Kurdjumov-Sachs (K-S) crystallographic orientation relationship of < 101 > FCC∥< 111 > BCC. Forming the thermodynamic perspective, such orientation relationship ensures the minimum interface energy between the two phases in the phase transition process, reduces the resistance of phase transformation, and significantly promotes the growth of BCC phase nuclei. It can be assumed that the dual-phase region is eutectic alloy solidification mode, with the two phases growing in an interdependent and competitive manner along a layer-by-layer stacking construction direction.Fig.7(c) schematically illustrates the dual-phase grains competition growth in the printing process. The already solidified portion under molten pool mode of will still undergo multiple thermal cycles of remelting and cooling, the Al vaporizes extensively with lower boiling point, and the generated recoil pressures drive the fluid motion in return, which tends to flow radially towards the heat-affected zone and its periphery [32]. The difference in composition causes concentrated nucleation growth of FCC and BCC grains in the re-melting and heat-affected zone and its periphery, respectively. Due to the barrier of phase boundary, both phase grains have difficulty to epitaxially growth into columnar crystals following the heat flow direction, which causes the unique equiaxed crystal distribution state.

Fig.9 The IPF map(a) and phase map(b) of printed Al0.52CoCrFeNi HEAs (Enlarged view including micro-areas). (c) Schematically illustrates formation of texture in printed dual-phase zone alloys.

3.4 Cracking behavior in BCC region

As shown in Fig.10, when added Al content exceeds 16 at.%, two kinds of coarse cracks are observed along different directions, both of which are about the size of 500um, cracking in LPBF-printed alloys severely deteriorates the properties. The vertical build direction is called delamination crack, which is generally considered to be related to residual stresses at the layer interfaces exceeding the yield strength of the alloy [30]. The solidification cracks parallel to the build direction mainly extend along the grain boundaries of large grains, the cracking behaviour is related to the liquefaction cracking caused by the large solidification and thermal shrinkage inherent in LPBF printing. The crack initiation and propagation behavior caused by excessive Al addition is analyzed in detail as follows. It is reported that due to the small atomic size difference among Co, Cr, Fe and Ni, the solid solution formed has high solubility and high structural stability, so when laser input energy into the molten pool, there is only thermal stress and volumetric stress caused by temperature gradient, but there is basically no internal stress caused by lattice distortion, resulting in excellent printability and extremely low hot cracking sensitivity of CoCrFeNi HEAs[47]. However, when Al with high heat loss rate and large atomic size radius is added in large quantities in CoCrFeNi HEAs, it will not only introduce a large number of lattice distortion, change the lattice constant and make the solid solution structure in a highly unstable state, but also significantly affect the solidification process. As the LPBF build is a non-equilibrium solidification process with repeated thermal and cold cycles, the average composition line of solid-liquid phase is far away from the liquid-solid phase line, the columnar grains growing in thermal gradient direction, leaving a laminar liquid at the interface where low melting point Al components are easily segregated. Trace additions of Al are less influential，and layered liquids rich in low melting point Al will gradually solidify down at lower temperatures. However, when Al is added above a certain value, thermodynamically the whole structure is in an unstable state, which is highly susceptible to rupture of the unstable liquid interdigitated regions, together with shrinkage, causing liquefaction cracking phenomena in the alloy, crack sprouting [48]. In addition, the phase transformation triggered by Al addition can have a huge impact on the stress distribution mechanism, the BCC phase grains suffer greater microscopic stresses and strains in dual-phase HEAs according to report, related to the higher dislocation density in the BCC phase [49]. Therefore, hot cracks once generated would propagate rapidly in the BCC phase in a across-grain manner. the FCC phase located at the boundary of BCC phase being a barrier to crack propagation. With the increase of Al content, the ductile FCC phase gradually decreases and the brittle BCC phase gradually increases in grain size, caused cracks to propagate rapidly. In summary, crack budding and propagation mechanisms due to temperature gradients, lattice distortions, and phase transitions lead to severe cracking in this LPBF-printed AlxCoCrFeNi compositional titer sample than Al0.75. Some work has investigated in detail the printing process window of equiatomic AlCoCrFeNi, the results showed that it was not possible to produce crack-free samples due to the combination of stresses generated during construction and phase transformations driven by high levels of Al biased to some extent. Reasonably variations in the chemical composition of alloys are required to reduce the phase transformations that occur during processing, only then could produce crack-free components [50].

Fig.10 EBSD Mapping(a) and IPF(b) of LPBF-printed indicating large scales of hot cracking, Al content higher than 16%.

3.5 Mechanical properties as a function of the Al concentration

Fig.11(a) shows the micro-hardness evolution of LPBF AlxCoCrFeNi (x from 0.04 to 0.75) gradient alloy. It can be found that the micro-hardness in the range of Al0.04-Al0.37 is stable at around 240 Hv. With further increase in Al content, the hardness gradually increases to around 300 Hv in the range Al0.5-Al0.6, indicating that the appearance of the BCC phase starts to harden the matrix. In the position range of Al0.6-Al0.75, the hardness suddenly increases sharply to over 400 Hv, up to about 520 Hv. Besides the BCC phase gradually replacing the FCC phase as the matrix phase in this region, hard secondary phases such as B2 phase are suspected to have precipitated, it was demonstrated can significantly increase matrix hardness in many reports[16][17].

In order to further investigate the effects of the phase distribution and compositional gradient on the mechanical properties of as-printed AlxCoCrFeNi alloys. The tensile properties are measured at different locations and plotted as a function of distance from the Al-rich as shown in Fig.11(b). Five representative composition intervals are selected, it can be seen that the ultimate tensile strength becomes higher with the increase of Al content. And the engineering stress-strain curves with different Al contents are given in Fig.11(c). The tensile strength of Al0.04 position interval is about 700Mpa, and the elongation is about 23.5%. There is little difference in tensile strength between Al0.17 and Al0.28, which is about 715Mpa. Compared with Al0.28, Al0.17 alloy exhibit high excellent elongation, which may be due to the slight lattice distortion caused by Minor addition of Al, helping the grains refine and arrange more densely, and improving elongation of the alloys to a certain extent. When the lattice distortion increases further with increasing Al, combined with the stress produced by LPBF thermal cycle, leading to a significant increase in defects. Fig.8 TEM results demonstrated the presence of numerous stacking faults and deformation dislocations. Deformation dislocation formation will change the distribution of Al as solute atoms, lead to a short-range ordered or partially aggregated state in the solid solution structure, which causing the system energy to rise, hindering the slip. With higher atomic number fractions of Al, the greater solid solution strengthening effect. The long-distance slip of dislocations is impeded, resulting in the decrease of elongation. The Al0.52 position region corresponds to the dual-phase region of FCC+BCC, the tensile strength increases obviously, and the elongation decreases only slightly compared with Al0.04 and Al0.17, which is attributed to the effective combination of ductile FCC phase and brittle BCC phase, the FCC provides plenty of space for slip to take place, while the BCC matrix phase provides high yield strength for alloys due to Al's strong solid solution strengthening. According to literature reports[51], synergistic deformation present in dual-phase structures can lead to extremely beneficial dynamic strain-stress distribution effects, reducing damage formation nucleation potential. Finally, elongation in the Al0.61 position range is significantly reduced, it related to the initiation and propagation of large pores and initial microcracks. Fig.9(c) shows tensile fracture morphology at different Al content positions. It can be seen that as Al content increases, the dominant fine craters of similar size to the honeycomb structure gradually decrease, indicating that ductile fracture behaviour is moderately suppressed with increasing Al content, and fracture behaviour gradually develops into brittle fracture. it can be seen that a similar crater structure is largely absent in Al0.7, which exhibits a typical brittle fracture surface with a regular deconstruction pattern and a river-like morphology.

Furthermore, the ultrafast cold solidification process of LPBF is often considered to help in obtaining fine microstructures with the sample. Fig.6(b) displays refined grain organization of the as-printed. This homogeneous and fine organization guarantees the superior mechanical properties of samples prepared using the LPBF process. The tensile properties of the AlCoCrFeNi-similar HEAs prepared by various preparation methods are summarized in Fig.11(d).The light yellow oval circle represents the tensile properties measured in this work, basically located in the upper left middle position, tensile strength is higher than most samples reported in the literature, and elongation have mostly remained above 20%. The trade-off between strength and elongation was achieved in the as-printed alloys with an Al0.52 composition.

Fig.10 Mechanical performance results for LPBF printed samples of AlxCoCrFeNi gradient alloys with different composition intervals. (a) Vickers hardness along the gradient direction (b) Tensile properties along the gradient direction, with distance from the Al-rich end. (c) Tensile engineering stress-strain curves forAl0.04, Al0.17, Al0.28, Al0.52, Al0.6 and Al0.7 alloys are given as representative; (d) Investigate and summarize the tensile strength and elongation. (FSP: Friction stir processing; SEBM: Selective electron beam melting; VIM: Vacuum induction melting.)

## 4. Conclusions

In this study, self-developed high-throughput laser powder bed fusion (LPBF) system was used to quickly established reference composition-structure-property experimental database, effectively enable the high-throughput screening of AlxCoCrFeNi HEA. And the unique effect of the fast heat and cold cycle was investigated for the LPBF manufacturing process on phase transformation, hardness and tensile properties in the high entropy alloy. Based on investigations in this study, the following conclusions were obtained：

- The addition of Al triggers the phase transition, and the system provides many nucleation sites for the BCC phase spontaneously for the relaxation strain energy, keeping the Al composition in the dual-phase region at around 8.5% to 14.5%, and LPBF's ultra-high cooling rate favours BCC phase formation, narrowing the composition region in which the phase transformation takes place.

- Overall compositional gradient sample construction direction columnar grains and subgrains are finer, which is attributed to LPBF's rapid solidification effect. The microstructure varies significantly with the one-dimensional increase of Al. The initial FCC matrix phase gradually transforms into the BCC phase. when the Al content is greater than about 14%, BCC becomes completely matrix phase, and spinodal decomposition produces minor B2 phase. In addition, Al addition has a refining effect on the FCC phase grains, which is attributed to the strong influence of lattice distortion and temperature gradient effects on grain refinement. At Al contents greater than 16%, the combination of residual stresses from the high rate of cold and heat cycling during LPBF layer-by-layer construction, the volumetric and thermal shrinkage effect of laminar liquid in the solidification region with increasing Al content, and the increased microscopic residual stresses enriched in the brittle BCC phase during the phase change provide the impetus for the widespread propagation of cracks across the grain, resulting in severe cracking behaviour in the high Al HEA specimens.

- With unique fine microstructure of the as-printed, results in an overall composition gradient alloy sample with excellent ductility while maintaining high strength hardness. As Al rises, solid solution strengthening becomes apparent, the hardness rising from around 220 Hv to 540 Hv. The sharp rise in hardness around 11% Al is associated with the BCC phase gradually taking over the main phase. The yield strength also rises gradually, but the elongation shows a fluctuating trend, which may be related to the lattice distortion caused by Al and the stress distribution between both phases. But excessive Al heat loss during the printing process and the excessive lattice distortion energy it brings promote the sprouting and extension of cracks, severely deteriorating material properties, thus near isoatomic ratios of AlCoCrFeNi HEA are not favored for additive manufacturing development. On balance, when the Al content is around 11% ± 1%, the alloy achieves a high hardness of 500 Hv, an ultimate tensile strength of 750 MPa and an excellent elongation of around 20%, successfully using the high throughput preparation concept to screen the composition range suitable for LPBF print forming of AlCoCrFeNi HEA powders.

## References

- J.-W. Yeh, S.-K. Chen, S.-J. Lin, J.-Y. Gan, T.-S. Chin, T.-T. Shun, C.-H. Tsau, S.-Y. Chang, Nanostructured High-Entropy Alloys with Multiple Principal Elements: Novel Alloy Design Concepts and Outcomes, 6(5) (2004) 299-303.

- B. Cantor, I.T.H. Chang, P. Knight, A.J.B. Vincent, Microstructural development in equiatomic multicomponent alloys, Materials Science and Engineering: A 375-377 (2004) 213-218.

- B. Gludovatz, A. Hohenwarter, D. Catoor, E.H. Chang, E.P. George, R.O. Ritchie, A fracture-resistant high-entropy alloy for cryogenic applications, Science 345(6201) (2014) 1153-1158.

- B. Gludovatz, A. Hohenwarter, K.V. Thurston, H. Bei, Z. Wu, E.P. George, R.O. Ritchie, Exceptional damage-tolerance of a medium-entropy alloy CrCoNi at cryogenic temperatures, Nat Commun 7 (2016) 10602.

- M.A. Hemphill, T. Yuan, G.Y. Wang, J.W. Yeh, C.W. Tsai, A. Chuang, P.K. Liaw, Fatigue behavior of Al0.5CoCrCuFeNi high entropy alloys, Acta Materialia 60(16) (2012) 5723-5734.

- Z. Tang, T. Yuan, C.W. Tsai, J.W. Yeh, C.D. Lundin, P.K. Liaw, Fatigue behavior of a wrought Al0.5CoCrCuFeNi two-phase high-entropy alloy, Acta Materialia 99 (2015) 247-258.

- S. Shafeie, S. Guo, Q. Hu, H. Fahlquist, P. Erhart, A. Palmqvist, High-entropy alloys as high-temperature thermoelectric materials, Journal of Applied Physics 118(18) (2015).

- Y. Shi, B. Yang, P. Liaw, Corrosion-Resistant High-Entropy Alloys: A Review, Metals 7(2) (2017).

- E.P. George, D. Raabe, R.O. Ritchie, High-entropy alloys, Nature Reviews Materials 4(8) (2019) 515-534.

- G.A. Salishchev, M.A. Tikhonovsky, D.G. Shaysultanov, N.D. Stepanov, A.V. Kuznetsov, I.V. Kolodiy, A.S. Tortika, O.N. Senkov, Effect of Mn and V on structure and mechanical properties of high-entropy alloys based on CoCrFeNi system, Journal of Alloys and Compounds 591 (2014) 11-21.

- J.M. Zhu, H.M. Fu, H.F. Zhang, A.M. Wang, H. Li, Z.Q. Hu, Synthesis and properties of multiprincipal component AlCoCrFeNiSix alloys, Materials Science and Engineering: A 527(27-28) (2010) 7210-7214.

- J.Y. He, H. Wang, H.L. Huang, X.D. Xu, M.W. Chen, Y. Wu, X.J. Liu, T.G. Nieh, K. An, Z.P. Lu, A precipitation-hardened high-entropy alloy with outstanding tensile properties, Acta Materialia 102 (2016) 187-196.

- Y.P. Lu, Y. Dong, S. Guo, L. Jiang, H.J. Kang, T.M. Wang, B. Wen, Z.J. Wang, J.C. Jie, Z.Q. Cao, H.H. Ruan, T.J. Li, A Promising New Class of High-Temperature Alloys: Eutectic High-Entropy Alloys, Sci Rep 4 (2014) 5.

- J. Gild, Y. Zhang, T. Harrington, S. Jiang, T. Hu, M.C. Quinn, W.M. Mellor, N. Zhou, K. Vecchio, J. Luo, High-Entropy Metal Diborides: A New Class of High-Entropy Materials and a New Type of Ultrahigh Temperature Ceramics, Sci Rep 6 (2016) 37946.

- J.-W. Yeh, Physical Metallurgy of High-Entropy Alloys, Jom 67(10) (2015) 2254-2261.

- Y. Zhang, T.T. Zuo, Z. Tang, M.C. Gao, K.A. Dahmen, P.K. Liaw, Z.P. Lu, Microstructures and properties of high-entropy alloys, Progress in Materials Science 61 (2014) 1-93.

- D.B. Miracle, O.N. Senkov, A critical review of high entropy alloys and related concepts, Acta Materialia 122 (2017) 448-511.

- W.-R. Wang, W.-L. Wang, S.-C. Wang, Y.-C. Tsai, C.-H. Lai, J.-W. Yeh, Effects of Al addition on the microstructure and mechanical property of AlxCoCrFeNi high-entropy alloys, Intermetallics 26 (2012) 44-51.

- Y. Zhang, Y.J. Zhou, J.P. Lin, G.L. Chen, P.K. Liaw, Solid-Solution Phase Formation Rules for Multi-component Alloys, Advanced Engineering Materials 10(6) (2008) 534-538.

- S. Guo, C. Ng, J. Lu, C.T. Liu, Effect of valence electron concentration on stability of fcc or bcc phase in high entropy alloys, Journal of Applied Physics 109(10) (2011).

- Y.-F. Kao, T.-J. Chen, S.-K. Chen, J.-W. Yeh, Microstructure and mechanical property of as-cast, -homogenized, and -deformed AlxCoCrFeNi (0≤x≤2) high-entropy alloys, Journal of Alloys and Compounds 488(1) (2009) 57-64.

- C. Zhang, F. Zhang, S. Chen, W. Cao, Computational Thermodynamics Aided High-Entropy Alloy Design, Jom 64(7) (2012) 839-845.

- A. Manzoni, H. Daoud, R. Volkl, U. Glatzel, N. Wanderka, Phase separation in equiatomic AlCoCrFeNi high-entropy alloy, Ultramicroscopy 132 (2013) 212-5.

- Z. Wang, S. Guo, C.T. Liu, Phase Selection in High-Entropy Alloys: From Nonequilibrium to Equilibrium, JOM 66(10) (2014) 1966-1972.

- C. Zhang, F. Zhang, H. Diao, M.C. Gao, Z. Tang, J.D. Poplawsky, P.K. Liaw, Understanding phase stability of Al-Co-Cr-Fe-Ni high entropy alloys, Materials & Design 109 (2016) 425-433.

- M. Kuczyk, L. Kotte, J. Kaspar, M. Zimmermann, C. Leyens, Alloy Design and Microstructure Evolution in the AlxCoCrFeNi Alloy System Synthesized by Laser Metal Deposition, Frontiers in Materials 7 (2020).

- U. Hecht, S. Gein, O. Stryzhyboroda, E. Eshed, S. Osovski, The BCC-FCC Phase Transformation Pathways and Crystal Orientation Relationships in Dual Phase Materials From Al-(Co)-Cr-Fe-Ni Alloys, Frontiers in Materials 7 (2020).

- Y. Shi, B. Yang, P.D. Rack, S. Guo, P.K. Liaw, Y. Zhao, High-throughput synthesis and corrosion behavior of sputter-deposited nanocrystalline Al (CoCrFeNi)100- combinatorial high-entropy alloys, Materials & Design 195 (2020).

- S.A. Kube, S. Sohn, D. Uhl, A. Datye, A. Mehta, J. Schroers, Phase selection motifs in High Entropy Alloys revealed through combinatorial methods: Large atomic size difference favors BCC over FCC, Acta Materialia 166 (2019) 677-686.

- T. DebRoy, H.L. Wei, J.S. Zuback, T. Mukherjee, J.W. Elmer, J.O. Milewski, A.M. Beese, A. Wilson-Heid, A. De, W. Zhang, Additive manufacturing of metallic components – Process, structure and properties, Progress in Materials Science 92 (2018) 112-224.

- C. Han, Q. Fang, Y. Shi, S.B. Tor, C.K. Chua, K. Zhou, Recent Advances on High-Entropy Alloys for 3D Printing, Adv Mater 32(26) (2020) e1903855.

- S.L. Sing, S. Huang, G.D. Goh, G.L. Goh, C.F. Tey, J.H.K. Tan, W.Y. Yeong, Emerging metallic systems for additive manufacturing: In-situ alloying and multi-metal processing in laser powder bed fusion, Progress in Materials Science 119 (2021).

- T. Borkar, B. Gwalani, D. Choudhuri, C.V. Mikler, C.J. Yannetta, X. Chen, R.V. Ramanujan, M.J. Styles, M.A. Gibson, R. Banerjee, A combinatorial assessment of AlxCrCuFeNi2 (0 < x < 1.5) complex concentrated alloys: Microstructure, microhardness, and magnetic properties, Acta Materialia 116 (2016) 63-76.

- M. Li, J. Gazquez, A. Borisevich, R. Mishra, K.M. Flores, Evaluation of microstructure and mechanical property variations in AlxCoCrFeNi high entropy alloys produced by a high-throughput laser deposition method, Intermetallics 95 (2018) 110-118.

- Y. Wen, B. Zhang, R.L. Narayan, P. Wang, X. Song, H. Zhao, U. Ramamurty, X. Qu, Laser powder bed fusion of compositionally graded CoCrMo-Inconel 718, Additive Manufacturing 40 (2021).

- N.T. Aboulkhair, M. Simonelli, L. Parry, I. Ashcroft, C. Tuck, R. Hague, 3D printing of Aluminium alloys: Additive Manufacturing of Aluminium alloys using selective laser melting, Progress in Materials Science 106 (2019).

- S. Singh, N. Wanderka, B.S. Murty, U. Glatzel, J. Banhart, Decomposition in multi-component AlCoCrCuFeNi high-entropy alloy, Acta Materialia 59(1) (2011) 182-190.

- L. Ma, C. Li, Y. Jiang, J. Zhou, L. Wang, F. Wang, T. Cao, Y. Xue, Cooling rate-dependent microstructure and mechanical properties of Al Si0.2CrFeCoNiCu1− high entropy alloys, Journal of Alloys and Compounds 694 (2017) 61-67.

- Y. Lv, R. Hu, Z. Yao, J. Chen, D. Xu, Y. Liu, X. Fan, Cooling rate effect on microstructure and mechanical properties of Al x CoCrFeNi high entropy alloys, Materials & Design 132 (2017) 392-399.

- D.H. StJohn, M. Qian, M.A. Easton, P. Cao, The Interdependence Theory: The relationship between grain formation and nucleant selection, Acta Materialia 59(12) (2011) 4907-4921.

- C.-J. Tong, Y.-L. Chen, J.-W. Yeh, S.-J. Lin, S.-K. Chen, T.-T. Shun, C.-H. Tsau, S.-Y. Chang, Microstructure characterization of AlxCoCrCuFeNi high-entropy alloy system with multiprincipal elements, Metallurgical and Materials Transactions A 36(4) (2005) 881-893.

- J.Y. He, W.H. Liu, H. Wang, Y. Wu, X.J. Liu, T.G. Nieh, Z.P. Lu, Effects of Al addition on structural evolution and tensile properties of the FeCoNiCrMn high-entropy alloy system, Acta Materialia 62 (2014) 105-113.

- J.C. Rao, H.Y. Diao, V. Ocelík, D. Vainchtein, C. Zhang, C. Kuo, Z. Tang, W. Guo, J.D. Poplawsky, Y. Zhou, P.K. Liaw, J.T.M. De Hosson, Secondary phases in AlxCoCrFeNi high-entropy alloys: An in-situ TEM heating study and thermodynamic appraisal, Acta Materialia 131 (2017) 206-220.

- X.Z. Gao, Y.P. Lu, B. Zhang, N.N. Liang, G.Z. Wu, G. Sha, J.Z. Liu, Y.H. Zhao, Microstructural origins of high strength and high ductility in an AlCoCrFeNi2.1 eutectic high-entropy alloy, Acta Materialia 141 (2017) 59-66.

- F. Otto, A. Dlouhý, C. Somsen, H. Bei, G. Eggeler, E.P. George, The influences of temperature and microstructure on the tensile properties of a CoCrFeMnNi high-entropy alloy, Acta Materialia 61(15) (2013) 5743-5755.

- M.K. Alam, M. Mehdi, R.J. Urbanic, A. Edrisy, Electron Backscatter Diffraction (EBSD) analysis of laser-cladded AISI 420 martensitic stainless steel, Materials Characterization 161 (2020).

- Y. Brif, M. Thomas, I. Todd, The use of high-entropy alloys in additive manufacturing, Scripta Materialia 99 (2015) 93-96.

- J.H. Martin, B.D. Yahata, J.M. Hundley, J.A. Mayer, T.A. Schaedler, T.M. Pollock, 3D printing of high-strength aluminium alloys, Nature 549(7672) (2017) 365-369.

- E. Ghassemali, R. Sonkusare, K. Biswas, N.P. Gurao, In-situ study of crack initiation and propagation in a dual phase AlCoCrFeNi high entropy alloy, Journal of Alloys and Compounds 710 (2017) 539-546.

- D. Karlsson, A. Marshal, F. Johansson, M. Schuisky, M. Sahlberg, J.M. Schneider, U. Jansson, Elemental segregation in an AlCoCrFeNi high-entropy alloy – A comparison between selective laser melting and induction melting, Journal of Alloys and Compounds 784 (2019) 195-203.

- Z. Li, K.G. Pradeep, Y. Deng, D. Raabe, C.C. Tasan, Metastable high-entropy dual-phase alloys overcome the strength-ductility trade-off, Nature 534(7606) (2016) 227-30.

- Z. Tang, O.N. Senkov, C.M. Parish, C. Zhang, F. Zhang, L.J. Santodonato, G. Wang, G. Zhao, F. Yang, P.K. Liaw, Tensile ductility of an AlCoCrFeNi multi-phase high-entropy alloy through hot isostatic pressing (HIP) and homogenization, Materials Science and Engineering: A 647 (2015) 229-240.

- H. Zheng, R. Chen, G. Qin, X. Li, Y. Su, H. Ding, J. Guo, H. Fu, Phase separation of AlCoCrFeNi2.1 eutectic high-entropy alloy during directional solidification and their effect on tensile properties, Intermetallics 113 (2019) 106569.

- T. Xiong, S. Zheng, J. Pang, X. Ma, High-strength and high-ductility AlCoCrFeNi2.1 eutectic high-entropy alloy achieved via precipitation strengthening in a heterogeneous structure, Scripta Materialia 186 (2020) 336-340.

- T. Wang, M. Komarasamy, S. Shukla, R.S. Mishra, Simultaneous enhancement of strength and ductility in an AlCoCrFeNi2.1 eutectic high-entropy alloy via friction stir processing, Journal of Alloys and Compounds 766 (2018) 312-317.

- K. Kuwabara, H. Shiratori, T. Fujieda, K. Yamanaka, Y. Koizumi, A. Chiba, Mechanical and corrosion properties of AlCoCrFeNi high-entropy alloy fabricated with selective electron beam melting, Additive Manufacturing 23 (2018) 264-271.

- L. Huang, Y. Sun, A. Amar, C. Wu, X. Liu, G. Le, X. Wang, J. Wu, K. Li, C. Jiang, J. Li, Microstructure evolution and mechanical properties of AlxCoCrFeNi high-entropy alloys by laser melting deposition, Vacuum  (2020) 109875.

- X. Gao, Y. Lu, B. Zhang, N. Liang, G. Wu, G. Sha, J. Liu, Y. Zhao, Microstructural origins of high strength and high ductility in an AlCoCrFeNi2.1 eutectic high-entropy alloy, Acta Materialia 141 (2017) 59-66.

- I.S. Wani, T. Bhattacharjee, S. Sheikh, P.P. Bhattacharjee, S. Guo, N. Tsuji, Tailoring nanostructures and mechanical properties of AlCoCrFeNi2.1 eutectic high entropy alloy using thermo-mechanical processing, Materials Science and Engineering: A 675 (2016) 99-109.